## Slide 1: Mobile Customers Feedback Summary Report from 2011/2012 Industry Data Collection (WW46 2011)
Prepared by:
SA Moy
Contributed by:
KK Tang

## Slide 2: Objectives
Share Findings from CME Mobile Industry Data Collection (Shark Bay Platform Survey)
    Summarize data collected from the Mobile Customers manufacturers (Quanta, Compal, Wistron, Inventec and Pegatron)
    Highlight key learning in focus areas of 2013 Platform (Shark Bay Platform).
Assist Internal Stakeholder better Alignment with Industry
    Provide data & analysis to aid in future platform enabling and Technology Risk Assessments
    Influence internal technology development direction toward more customer oriented

## Slide 3: Summary of Survey
A). PCB Technology
No standard size of board form factor, rectangle is common but the size is different. Quanta (Dell, Toshiba, NEC) is using dual boards.
The Minimum Layers Count is 2 (from Compal) and Maximum Layers Count is 8 (from Inventec). 6 Layers are the most common and widely used by Quanta, Wistron and Inventec.
The Minimum Board Thickness is 1mm (from Compal and Inventec) and Maximum Board Thickness is 1.2mm (from Quanta, Wistron and Inventec). 1.2mm Board Thickness is the most common used at ODMs.
OSP is the only surface finish used by ODMs.
B). Screen Pritning
The Minimum Stencil Thickness is 0.08mm (3.15mil) and Maximum Stencil Thickness is 0.13mm (5.12mil). The most common stencil thickness is range from 0.12-0.13mm (4.72-5.12mil).
Shenmao (PF606-P) is the most common solder paste at ODMs. Wistron-Lenovo is using Alpha OM338 which is suspected high risk for hanging call issue. Low Ag solder paste (PF629-P) is next trend coming soon (using for small OEMs now). [KOKI-Local OEM]
C). Placement
ODMs are using PnP machines which has 100% solder ball recognition capability.
D). Reflow
Different reflow machine type been used by ODMs. All ODMs are using N2 reflow. Inventec and Pegatron reply <1000 O2 ppm, others didn’t disclose detail.
All ODMs are using reflow pallet. Aluminum is the material common used and only Pagatron is using Glass Fiber, Epoxy Resin.
The Minimum belt speed is 100 cm/min (from Compal) and the Maximum is 160 cm/min (from Wistron). 120 cm/min belt speed is the most common used by ODMs.
The minimum peak is 230 deg C and the maximum is 255 deg C. The minimum TAL is 40 sec and maximum is 90 sec. Majority is following soak time 60-120 sec and Inventec is following soak time 60-90sec.

## Slide 4: Summary of Survey
E). Rework
Different Brand and Model of rework machine used at ODMs (Martin, DIC and Quick) . None of ODMs using SRT.
4/8 using solder paste during rework and 4/8 using flux. Same type of solder paste in SMT been used for rework (Shenmao PF606-P).
4/8 customers are using manual component placement and expected at least >85% yield. Pegatron’s reply manual placement and yield is 99.85%.
F). Glue
All customers have corner glue process and capability. Wistron is practicing dot shape corner glue and Inventec is practicing L-Shape. Others customers didn’t disclose details.
Loctite 3705 UV cure is widely used. Other brand like Panasonic (ADE480D-1), DYMAX, Loctite 3619 and Loctite 3620 are also common adhesive material.
Different brand of equipment/dispenser been used. Only Inventec reply it is manual dispenser. There is no details sharing by other ODMs.

## Slide 5: Contents
PCB Technology
Screen Pritning
Placement
Reflow
Rework
Glue

## Slide 6: PCB Technology

## Slide 7
No | Segment (Mobile/Table/Smart Phone/Mobile/Server | Customer Name | OEM (Key in Company name) | Board Form Factor | 
 |  |  |  | Shape | Size
 | Mobile | Quanta | Dell | Rectangle, dual board | 410*245mm
 | Mobile | Quanta | Toshiba | Rectangle, dual board | 390*258mm
 | Mobile | Quanta | NEC | Rectangle, dual board | 259*217mm
 | Mobile |  | Wistron | Rectangular | 202* 202mm
 | Mobile |  | Compal | Rectangular | 350mm
 | Mobile |  | Inventec | Odd Shape | >8" x 8"
 | Mobile |  | Inventec | Single panel/ Square | 177.5X233.2mm
 | Mobile |  | Pegatron |  | 
Board Form Factor
No standard size of board form factor, although it is rectangle but the size is different.
Quanta is using Rectangle shape with dual boards.

## Slide 8
No | Segment (Mobile/Table/Smart Phone/Mobile/Server | Customer Name | OEM (Key in Company name) | Board Layers Count
 | Mobile | Quanta | Dell | 6
 | Mobile | Quanta | Toshiba | 6
 | Mobile | Quanta | NEC | 6
 | Mobile |  | Wistron | 6
 | Mobile |  | Compal | 2
 | Mobile |  | Inventec | 8
 | Mobile |  | Inventec | 6
 | Mobile |  | Pegatron | 
Board Layers Count
The Minimum layers count is 2 (from Compal) and Maximum layers count is 8 (from Inventec).
6 layers are the most common and widely used by Quanta, Wistron and Inventec.

## Slide 9
No | Segment (Mobile/Table/Smart Phone/Mobile/Server | Customer Name | OEM (Key in Company name) | Board Thickness
 | Mobile | Quanta | Dell | 47.2±5mil (1.2 ± 0.127 mm)
 | Mobile | Quanta | Toshiba | 47.2±5mil (1.2 ± 0.127 mm)
 | Mobile | Quanta | NEC | 47.2+/-5 MIL (1.2 ± 0.127 mm)
 | Mobile |  | Wistron | 1.2mm
 | Mobile |  | Compal | 1mm
 | Mobile |  | Inventec | 1.2mm~1.0mm
 | Mobile |  | Inventec | 1.2mm
 | Mobile |  | Pegatron | 
Board Thickness
The Minimum Board Thickness is 1mm (from Compal and Inventec) and Maximum Board Thickness is 1.2mm (from Quanta, Wistron and Inventec).
1.2mm Board Thickness is the most common used at ODMs.

## Slide 10
No | Segment (Mobile/Table/Smart Phone/Mobile/Server | Customer Name | OEM (Key in Company name) | Surface Finish
 |  |  |  | Surface Type
 | Mobile | Quanta | Dell | OSP
 | Mobile | Quanta | Toshiba | OSP
 | Mobile | Quanta | NEC | OSP
 | Mobile |  | Wistron | OSP
 | Mobile |  | Compal | OSP
 | Mobile |  | Inventec | OSP
 | Mobile |  | Inventec | OSP
 | Mobile |  | Pegatron | 
Surface Finish
OSP is the only surface finish used by ODMs.

## Slide 11: Screen Printing

## Slide 12
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | What is the stencil thickness
 |  |  | Stencil Thickness (mm)
 | Mobile | Quanta-Dell | 0.12
 | Mobile | Quanta-Toshiba | 0.12
 | Mobile | Quanta-NEC | 0.12
 | Mobile | Wistron-HP | 0.127
 |  | Wistron-Dell | 0.127
 |  | Wistron-Acer | 0.127
 |  | Wistron-HP | 0.127
 |  | Wistron-Dell | 0.127
 |  | Wistron-Acer | 0.127
 |  | Wistron-Lenovo | 0.127
 | Mobile | Compal | 0.08
 |  | Compal | 0.1
 |  | Compal | 0.13
 |  | Compal | 0.15
 | Mobile | Inventec | 0.127
 | Mobile | Inventec | 0.13
 | Mobile | Pegatron | 0.13
Stencil Thickness
The minimum stencil thickness is 0.08mm (3.15mil) and maximum is 0.13mm (5.12mil).
The most common stencil thickness is range from 0.12-0.13mm (4.72-5.12mil).

## Slide 13
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Solder Paste used |  |  | 
 |  |  | Brand | Model | Alloy | Powder Type
 | Mobile | Quanta-Dell | Shenmao | PF606-P | SAC305 | 4
 | Mobile | Quanta-Toshiba | Shenmao | PF606-P | SAC305 | 4
 | Mobile | Quanta-NEC | Shenmao | PF606-P | SAC305 | 4
 | Mobile | Wistron-HP | SENJU | M705-S101ZH-S4 | SAC305 | 4
 |  | Wistron-Dell | SENJU | M705-S101ZH-S4 | SAC305 | 4
 |  | Wistron-Acer | SENJU | M705-S101ZH-S4 | SAC305 | 4
 |  | Wistron-HP | Shenmao | PF606-P | SAC305 | 4
 |  | Wistron-Dell | Shenmao | PF606-P | SAC305 | 4
 |  | Wistron-Acer | Shenmao | PF606-P | SAC305 | 4
 |  | Wistron-Lenovo | Alpha | OM388 |  | 
 | Mobile | Compal | Shenmao | PF606-P | SAC305 | 4
 |  | Compal |  |  |  | 
 |  | Compal |  |  |  | 
 |  | Compal |  |  |  | 
 | Mobile | Inventec | Shenmao | PF606-P | SAC305 | 4
 | Mobile | Inventec | Shenmao | PF606-P | SAC305 | 4
 | Mobile | Pegatron | Shenmao | FORMAOSA PF606-P 20-38 flux:ROL1 | Sn/Ag3.0/Cu0.5/x | 4
Solder Paste
Chart: 
| Shenmao PF606-P | Senju M705-S101ZH-S4 | Alpha OM388
Solder Paste Brand & Model | 10 | 3 | 1
Shenmao (PF606-P) is the most common solder paste at ODMs.
Wistron-Lenovo is using Alpha OM388 which is suspected high risk for hanging call issue.

## Slide 14
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Please list the Screen Print Machine used | 
 |  |  | Vendor | Model
 | Mobile | Quanta-Dell | Panasonic | SP28
 | Mobile | Quanta-Toshiba | Panasonic | SP60
 | Mobile | Quanta-NEC | FUJI | GP641E
 | Mobile | Wistron-HP | DEK | Horizon APiX
 |  | Wistron-Dell |  | 
 |  | Wistron-Acer |  | 
 |  | Wistron-HP |  | 
 |  | Wistron-Dell |  | 
 |  | Wistron-Acer |  | 
 |  | Wistron-Lenovo |  | 
 | Mobile | Compal | DEK | Infinite
 |  | Compal |  | 
 |  | Compal |  | 
 |  | Compal |  | 
 | Mobile | Inventec | MPM / DEK | Momentun elite / Infinity Api
 | Mobile | Inventec | DEK | DEK-Infinity AP
 | Mobile | Pegatron | FUJI&DEK | FUJI GPX&DEK INFINITY
Screen Print Machine

## Slide 15
Chart: Stencil Thickness (unit in mm)
| Quanta-Dell | Quanta-Toshiba | Quanta-NEC | Wistron-HP | Wistron-Dell | Wistron-Acer | Wistron-Lenovo | Compal | Compal | Compal | Compal | Inventec | Inventec | Pegatron
Stencil Thickness | 0.12 | 0.12 | 0.12 | 0.127 | 0.127 | 0.127 | 0.127 | 0.08 | 0.1 | 0.13 | 0.15 | 0.127 | 0.13 | 0.13
Chart: 
| Shenmao PF606-P | Senju M705-S101ZH-S4 | Alpha OM388
Solder Paste Brand & Model | 10 | 3 | 1

## Slide 16: Placement

## Slide 17
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Please list the BGA Placement Machine used |  | 
 |  |  | Vendor | Model | 100% Ball Recognition?
 | Mobile | Dell | Panasonic | CM402-L | YES
 | Mobile | Toshiba | Panasonic | DT401 | YES
 | Mobile | NEC | FUJI | QP341/QP351 | YES
 | Mobile | Wistron | Panasonic | DT401 | YES
 | Mobile | Compal | Panasonic | DT401 | YES
 | Mobile | Inventec | Panasonic | DT401 / CM602 B TYPE | YES
 | Mobile | Inventec | Panasonic/Universal-GSM | DT401 / CM602 B TYPE/OSP/Windows | YES
 | Mobile | Pegatron | FUJI | FUJI NXT M6 | YES
BGA Placement Machine
Panasonic, Fuji and Universal (GSM) are the PnP machines used by ODMs.
All of them has 100% solder ball recognition capability.

## Slide 18: Reflow

## Slide 19
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Q1: Reflow Machine's |  | Q2: N2 reflow? | Q3: O2 ppm level
 |  |  | Brand | Model |  | 
 | Mobile | Quanta-Dell | 超越 | CHA-400 N2-14CF | Yes | 
 | Mobile | Quanta-Toshiba | TAMURA | TNR-6910PH | Yes | 
 | Mobile | Quanta-NEC | TAMURA | TNR-6910PH | Yes | 
 | Mobile | Wistron | Rehm | VXs-944 | Yes | 
 | Mobile | Compal | BTU | Prymax | Yes | 
 | Mobile | Inventec-HP | REMH | V7/ V8/ V9/ VXS944 | Yes | <1000
 | Mobile | Inventec-Toshiba | REMH/HELLER | V7/ V8/ V9/ VXS944/1900EXI | Yes | <1000
 | Mobile | Pegatron | WAVE POINT & TAMURA | CHA-400N2-1767CF&TNP50-6910PM | Yes | <1000
Reflow Machine, N2 and O2 ppm Level
Different reflow machine type been used by ODMs.
All ODMs are using N2 reflow. Inventec and Pegatron reply <1000 O2 ppm, others didn’t disclose detail.

## Slide 20
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | With Pallet / Carrier? |  | 
 |  |  | Yes / No | Product specific / generic pallet? | What material used for Pallet fabrication?
 | Mobile | Quanta-Dell | Yes | Product specific | AL alloy
 | Mobile | Quanta-Toshiba | Yes | Product specific | AL alloy
 | Mobile | Quanta-NEC | Yes | Product specific | AL alloy
 | Mobile | Wistron | Yes | Product specific | Aluminium
 | Mobile | Compal | Yes | Both | Aluminium alloy
 | Mobile | Inventec-HP | Yes | generic pallet | Aluminum
 | Mobile | Inventec-Toshiba | Yes | generic pallet | Aluminum
 | Mobile | Pegatron | Yes | N/A | GLASS FIBER,EPOXY RESIN
Reflow Pallet and Material
All ODMs are using reflow pallet.
Quanta and Wistron’s pallets design are product specific. Inventec is using generic pallet and Compal has both.
Aluminum is the material common used and only Pagatron is using Glass Fiber, Epoxy Resin.

## Slide 21
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Belt Speed (cm/minute)
 | Mobile | Quanta-Dell | 120
 | Mobile | Quanta-Toshiba | 120
 | Mobile | Quanta-NEC | 120
 | Mobile | Wistron | 160
 | Mobile | Compal | 100
 | Mobile | Inventec-HP | 120
 | Mobile | Inventec-Toshiba | 120
 | Mobile | Pegatron | 120
Belt Speed
Chart: Reflow Machine Belt Speed (cm/min)
| Quanta-Dell | Quanta-Toshiba | Quanta-NEC | Wistron | Compal | Inventec-F5 | Inventec-F1 | Pegatron
Reflow Machine Belt Speed | 120 | 120 | 120 | 160 | 100 | 120 | 120 | 120
The minimum belt speed is 100 cm/min (from Compal) and the maximum is 160 cm/min (from Wistron).
120 cm/min belt speed is the most common used by ODMs.

## Slide 22
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Peak temperature (°C) | TAL | Soak Time | Max Rising Slope | Max Falling Slope
 | Mobile | Quanta-Dell | 235-255 | 40-70 s | 60-120 | 3°C/s | -6°C/s
 | Mobile | Quanta-Toshiba | 235-250 | 40-70 s | 60-120 | 3°C/s | -6°C/s
 | Mobile | Quanta-NEC | 235-250 | 40-70 s | 60-120 | 3°C/s | -6°C/s
 | Mobile | Wistron | 230-250 | 40-90 s | 60-120 | 1-3°C/s | >1°C/s
 | Mobile | Compal | 240-250 | 45-90 s | 60-120 | 3 | 3
 | Mobile | Inventec-HP | 235-245 | 60-90 s | 60-90 | ≤3°C/s | <-4°C/s
 | Mobile | Inventec-Toshiba | 235-245 | 60-80 s | 60-90 | ≤3°C/s | <-3°C/s
 | Mobile | Pegatron | 235-243 | 40-70 s | 60-120 | 3°C/s | -3°C/s
Reflow Profile Parameters
Quanta-Dell
Wistron
Peak (°C)
TAL (sec)
230
240
250
40
50
60
70
80
90
Quanta-Dell
Quanta-NEC
Compal
Inventec-HP
Inventec-Toshiba
Pegatron
The lowest peak is 230 deg C and the maximum is 255 deg C.
The minimum TAL is 40 sec and maximum is 90 sec.
Majority is following soak time 60-120sec and Inventec is following 60-90sec.

## Slide 23: Rework

## Slide 24
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Q1: Rework Machine | 
 |  |  | Brand | Model
 | Mobile | Dell | MARTIN | MT7000
 | Mobile | Toshiba | MARTIN | MT7000
 | Mobile | NEC | MARTIN | MT7000
 | Mobile | Wistron | DIC | RD500III
 | Mobile | Compal | RD500 | RD500
 | Mobile | Inventec | QUICK | 2015
 | Mobile | Inventec | QUICK | 2015
 | Mobile | Pegatron | DIC | RD-500
Rework Machine
Different Brand and Model (Martin, DIC and Quick) of rework machine used at ODMs.
None of ODMs using SRT.

## Slide 25
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Do you use solder paste or flux for rework? What brand and model used? |  | 
 |  |  | Solder Paste or Flux | Brand | Model
 | Mobile | Dell | Solder Paste | Shenmao | PF606-P
 | Mobile | Toshiba | Solder Paste | shenmao | PF606-P
 | Mobile | NEC | Solder Paste | shenmao | PF606-P
 | Mobile | Wistron | Flux | Solder paste: SENJU Flux: Shenmao | Solder paste:M705-S101ZH-S4 / Flux: SMF-2
 | Mobile | Compal | Flux | Shenmao | SMF-2
 | Mobile | Inventec | Flux | AMTECH | NC559ASM
 | Mobile | Inventec | Flux | AMTECH | NC560ASM
 | Mobile | Pegatron | Solder Paste | Shenmao | FORMAOSA PF606-P 20-38 Flux:ROL1
Solder Paste and Flux for Rework
4/8 using solder paste during rework and 4/8 using flux.
Same type of solder paste in SMT been used for rework (Shenmao PF606-P).

## Slide 26
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Component placement placement is manual or by machine | Rework Yield?
 | Mobile | Dell | Hand | >85%
 | Mobile | Toshiba | Hand | >85%
 | Mobile | NEC | Hand | >85%
 | Mobile | Wistron | Auto | >95%
 | Mobile | Compal | Auto/Hand | 98%
 | Mobile | Inventec | Auto/Hand | ≤90%
 | Mobile | Inventec | Auto/Hand | ≤90%
 | Mobile | Pegatron | Hand | 99.85%
Component Placement and Rework Yield
4/8 customers are using manual component placement.
Expected at least >85% yield.
Pegatron’s reply manual placement and yield is 99.85%.

## Slide 27: Glue

## Slide 28
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Adhesive/Glue application processes. (Underfill / Corner Glue / Other) | Q2: Reworkable / Non-reworkable adhesive material selection
 | Mobile | Dell | Corner Glue | 
 | Mobile | Toshiba | Corner Glue | 
 | Mobile | NEC | Corner Glue | 
 | Mobile | Wistron | dots on corner | 
 | Mobile | Compal | Corner Glue | 
 | Mobile | Inventec | L shaped corner glue | 
 | Mobile | Inventec | L shaped corner glue | 
 | Mobile | Pegatron |  | 
Corner Glue / Underfill / Other
All customers have corner glue process and capability
Wistron is practicing dot shape corner glue and Inventec is practicing L-Shape. Others customers didn’t disclose details.

## Slide 29
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Adhesive Material |  | 
 |  |  | Brand | Cure Type | Model
 | Mobile | Dell | Loctite/Eict | UV | Loctite 3705/Eict UV-3200
 | Mobile | Toshiba | Loctite/Eict | UV | Loctite 3705/Eict UV-3200
 | Mobile | NEC | Loctite/Eict | UV | Loctite 3705/Eict UV-3200
 | Mobile | Wistron | Panasonic |  | ADE480D-1
 | Mobile | Compal | Loctite/Eict |  | 3705
 | Mobile | Inventec | LOCTITE |  | L3619
 | Mobile | Inventec | LOCTITE |  | L3620
 | Mobile | Pegatron | DYMAX |  | 3069-GEL-ASUS
Adhesive Material
Loctite 3705 UV cure is widely used.
Other brand like Panasonic (ADE480D-1), DYMAX, Loctite 3619 and Loctite 3620 are also common adhesive material.

## Slide 30
No | Segment (Mobile/UMG(PoP)/Mobile | Customer | Equipment/Dispenser Manufacturer and Model | 
 |  |  | Brand | Model
 | Mobile | Dell | EM-5701N Dispenser | EM-5701N Dispenser
 | Mobile | Toshiba | EM-5701N Dispenser | 
 | Mobile | NEC | EM-5701N Dispenser | 
 | Mobile | Wistron | HTD/Camalot | 
 | Mobile | Compal | 億力 | 
 | Mobile | Inventec | QUICK ST-982 (Manual Dispenser) | 
 | Mobile | Inventec | QUICK ST-982 (Manual Dispenser) | 
 | Mobile | Pegatron | MUSASHI SHOTMASTOR | 
Equipment/Dispenser Manufacturer and Model
Different brand of equipment/dispenser been used. Only Inventec reply it is manual dispenser. There is no details sharing by others.