## Slide 1: SMT Process Gaps ODM vs Intel Process Dev
Todd Harris – CPTD
Ack: SA Moy, Mukul Sakalkale

## Slide 2
Several gaps have been identified btw ODM high volume SMT assembly and Intel Oregon process development.
  Clamp vs No-clamp reflow pallets
  Peak temp for BGA
  Solder Paste Brand.
  Print Speed
ODMs are widening their SMT process window to reduce costs and increase throughput.
Intel is optimizing the SMT process window for packages with increased warpage and variability.
Need to align on what is communicated in MAS.
  Optimized reference process or ODM envelope
Overview

## Slide 3
Background
ODMs use automated equipment to load PCBs into pallets. Clamping the edge of PCB is not possible. This is driven by cost savings.
Intel clamps the PCB to reduce BGA area warpage to <50um.
PCB design is main influence on PCB warpage. (Thickness, Stackup, etc)
Status:
BDW YTB clamp vs no clamp shadow moire showed 2X increase in PCB warpage for BGA area.
ODMs are not enabled to measure their PCB warpage.
Next Steps:
Collect PCB warpage data on Haswell Compal & Wistron ODM boards
CME to collect bare Compal BDW PCBs and Pallet design info.
Modeling to determine impact of increased YTB warpage
SMT build comparing clamp to no clamp
Clamp vs. No Clamp

## Slide 4
Background
ODMs use the full range of 230 – 250 degC for reflow. Multiple board designs are run on the same reflow oven settings to reduce changeover.
Intel recommends 235-245 degC for reflow to provide the optimized reflow conditions.
Status:
Intel tested 235-245 for BDW MAS development.
ODM data from Moy (CME) shows acceptable yields at both 230 and 250 for the BDW ULX BGA.
Next Steps:
Determine need for BDL DOE testing at 230 and 250 Peak Temp.
Review ODM data from Moy
Align on MAS communication.
  235-245 degC or 230-250 degC
Peak Reflow Temp

## Slide 5
Background
Yunnan Tin is a lower cost solder paste being considered by multiple ODMs for high volume assembly.
BDL completed two SMT builds with Yunnan Tin with positive results. The Paste Screening test for MAS has not been completed.
Status:
Only 1 or 2 ODMs use Yunnan Tin but CME projects it will gain MS.
Internal alignment that Yunnan Tin will not be included in BDW MAS. May intercept Sky Lake based on future ODM MS.
Next Steps:
Materail Property Analysis of Yunnan Tin - Lilia
Track ODM usage by MS and ODM - CME
Solder Paste

## Slide 6
Background
ODMs print faster due to SMT line beat rate. Typically 80-120cm/min.
BDL process development was completed with slower print speeds for achieving better print quality. Typically 20cm/min.
Need to align print speeds to ensure BDL stencils designs are usable in the HVM environment.
Status:
Cliff / Industry DOE was completed with a print speed to 80cm/min. Print quality met paste volume requirements.
Next Steps:
Align future BDL process development to higher print speeds. Likely 80cm/min
Paste Print Speed

## Slide 7
Align on MAS recommendations
  Deliver optimized SMT process or ODM envelope?
  SJQ MAS is available for process development enabling
CME to provide ODM’s process overview for no-clamp pallets and peak temperature.
Help Needed

## Slide 8: Back Up

## Slide 9
OEM Items |  | Intel MAS 1.0 |  |  |  |  |  |  | Notes
 | Parameters | NA | Wistron | Inventec | Asus/Quanta | Quanta (Lenovo Line) | Dell / Compal | Pegatron (Dell Line) | 
 | SOLDER PASTE PRINT |  |  |  |  |  |  |  | 
 | Stencil Thickness1 | 4 mils | 4 mils | 5 mils and 4 mils | 4 mils and 3 mils | 4 mil and 3 mil | 4 mil | 4 mil (0.10mm)and 3 mil (0.08mm) | 5 mil: Need to validate Apple stencil - please get from Eric & Mukul. 3 mil: Need to validate with same aperture with 4 mil in MAS.
 | Solder Paste1 | Alpha OM363*, Alpha OM363H*, Senju M705-GRN360-K2-VZH*, Senju M705-S101HF(N4)-S4*, Shenmao PF606-P*, Shenmao PF606-P26* | Senju M705-S101ZH-S4(W2) | Shenmao PF606-P | Shenmao PF606-P | Shenmao PF606-P | Shenmao & Yunnan Tin (YW9-3005-98CW04) | Shenmao PF606-P and Alpha OM338-L1 | Validate: 1). Senju M705-S101ZH-S4(W2) 2). Yunnan Tin (YW9-3005-98CW04) 3). Alpha OM338-L1
 | Stencil Aperture Design1 | Ref to MAS module 3 | Follow MAS 1.1 | Follow MAS 1.1 (both 5 mil and 4 mil) | 1:1 square and 1:1.3 square | Follow MAS 1.1 | Follow MAS 1.1 | Follow MAS 1.1 | 
 | Print Speed 2 | 23 mm/s | 70mm/s and 100mm/s | 80mm/s | 100mm/s | 200 mm/s | 130mm/s | 60mm/s | Print Speed impacts throughput and is Customer critical >>> What is the maximum printing speed that can meet with same aperture in MAS?
 | Print Pressure2 |  | 7 kg | 9 kg | 85N | 70N | 19 kg? | 6 kg | Print pressure impacts solder paste volume is Customer critical
 | Stencil Manufacturing Process |  | Laser Cut, Electropolish | Laser Cut, Electropolish | Laser Cut, Electropolish | Laser Cut, Electropolish | Laser Cut, Electropolish | Laser Cut, Electropolish | 
 | Separation Speed |  | 2mm/s | 3mm/s | 5mm/s | 3 mm/s | 1.0 mm/s | 1.0 mm/s | 
 | SOLDER PASTE INSPECTION |  |  |  |  |  |  |  | 
 | Paste Volume Control Limit 1, 2 | -/+50% | 40%～170% | 50% - 150% | 50%~+100% | Low:0.4*Stencil volume High: 1.8*Stencil volume | reduce 40%~ add 40% | 50%~190% | Wider range compare with Intel
 | Paste Height Control Limit 2 |  | 40%～170% | 50% - 150% | 50%~+100% | Low:0.4*Stencil area High:1.8*Stencil area | reduce 40%~ add 40% | 50%~190% | 
 | Paste Area Control Limit |  | 40%～170% | 50% - 150% | -30%~+80% | Low: 0.4*Stencil thickness High: 1.4*Stencil thickness | reduce 30%~ add 60% | 50%~190% | 
 | PNP |  |  |  |  |  |  |  | 
 | Component Placement 1 | 100 % Ball recognition | 100% | 100% |  | 100% | 100% | 100% | 
 | Nozzle Diameter 2 | Not Available | Dual Head, ID: 1mm | 5mm |  | 6mm | 6*4mm | 5.0mm | Critical --> customer need guidance if specialized nozzle have to used
 | Component Height (Pre-SMT) 2 |  | 0.3mm | 0.3mm |  | 1.8mm | 1.1mm | 1.08mm | Critical because not all equipment have force detection
 | Placement Speed 2 |  | 80mm/s | 40 |  | 40 | 80% | 7 | Placement speed impacts throughput - Customer critical
 | REFLOW |  |  |  |  |  |  |  | 
 | Peak Temp 1.2 | 235 - 245°C | 235～245℃ (HVM: 230-250deg C) | 235 - 250 deg C | 240.76~243.01 (HVM: 235 - 250 deg C) | 239~245 [HVM: 230 – 250 deg C] | 235 - 250 deg C | 230 - 250 deg C | Industry peak temperature is range from 230 - 250 deg C.
 | TAL 1,2 | 40 to 90 seconds for N2 (O2<3000 PPM) 60 -90 seconds for Air | 54 sec | 81.1S~89.0S(Long) / 70.6S~75.8S(Short) | 55 sec and 75 sec | 62~66 sec | Control: 45 - 90 sec | Running: 62.8 - 67.7 sec | 
 | Soak Temp and Time 1,2 | Paste dependent; follow paste manufacturer’s requirements | Control: 150 deg C - 180 deg C: <110s | Running: 155 - 185 deg C 61.6S~69.3S(Long)/60.6S~69.0S(Short) | Running: 155 - 185 deg C 92.07~93.60 | Running: 155~185 deg C for 78~86 sec | Control: 60 - 120 sec | Running: 150 - 185 deg C for 67.3 - 70.6 sec | 
 | Delta T 1,2 | Control ΔT across component to <10°C |  | <10 deg C | < 10 deg C | < 10 deg C | < 10 deg C | < 10 deg C | 
 | Pallet 1, 2 | Yes | Yes | Yes | Yes | Yes | Yes | Yes | 
 | Clamping / No Clamping 1,2 | Clamping | No | Yes | Special | No | No | No | Validate No clamp
 | Board Handling | Board is place in pallet after screen printing | boards manually placed in Reflow Pallets prior reflow | boards manually placed in Reflow Pallets prior reflow | boards manually placed in Reflow Pallets prior reflow | boards manually placed in Reflow Pallets prior reflow | boards manually placed in Reflow Pallets prior reflow | boards manually placed in Reflow Pallets prior reflow | Industry practice: boards manually placed in Reflow Pallets prior reflow
 | Belt Speed 2 | ?? | 100 cm/min | 120 cm/min | 110 cm/min | 120 cm / min | 110 cm / min | 1.10 cm/min | Belt speed: 100 cm/min - 120 cm/min
 | N2 1 | N2 (02<3000 PPM). Air is acceptable | N2 | N2 | N2, O2:4500±300DPPM | N2, O2: 5000 PPM | N2 and Air | N2 3000 ppm | N2 and Air (some ODMs are looking for cost saving now).
Ack: SA Moy

## Slide 10: Fundamental Understanding of Materials Differences
Alpha OM363 and Shenmao PF606-P26 with various viscosity skews
Measurement | Test Location | Status
Viscosity as f(T) | AMCL | WO # 803343, Materials delivered, ECD – WW16
Tackiness as f(T) | AMCL | WO # 803344, Materials delivered, ECD – WW16
Paste slump (RT/HT) | Suppliers Data (IPC-TM- 650) | Shenmao – Done Alent – WiP
Paste Activity | -AMCL – Rhesca on Cu wire -AMCL – Solder spread -PL – Sn dissolution/sintering | -WO # 803346, Materials delivered, ECD – WW16 -WO # 803347, Materials delivered, ECD – WW16 - QTM in place, ECD – WW15
TGA Wt loss & onset Temp | AMCL | WO # 803349, Materials delivered, ECD – WW16
DSC Melting & Solidification | AMCL | WO # 803348, +Materials delivered, ECD – WW16
Ack: Lilia May