## Slide 1: Mobile Customers Equipment Summary Report
Prepared by:
SA Moy

## Slide 2: Objectives
Share Findings from CME Mobile Industry Data Collection (Sky Lake Platform Survey)
    Summarize data collected from the Mobile Customers manufacturers (Quanta, Compal, Wistron, Inventec, Pegatron and others)

## Slide 3: Screen Printing

## Slide 4
No | Customer | What is the stencil thickness
 | Compal CQ (Acer) | 4 mil and 5 mil
 | Quanta CQ (F1 Building) | 0.1mm
 | Wistron CD | 4 mil
 | Wistron KS | 4mil
 | Compal KS (Dell) | 4 mil
 | LCFC | 0.10mm
Stencil Thickness

## Slide 5
No | Customer | Solder Paste used |  |  | 
 |  | Brand | Model | Alloy | Powder Type
 | Compal CQ (Acer) | Shenmao | PF606-P | SAC305 | Type 4
 | Compal KS (Dell) | Yun Nan Tin | YW9-3005-98CY04 | SAC305 | Type 4
 | Quanta SH (Asus) | Shenmao | PF606-P | SAC305 | Type 4
 | Quanta CQ (F1 Building) | Shenmao | PF606-P | SAC305 | Type 4
 | Wistron CD | Shenmao | PF606-PC | SAC305 | Type 4
 | LCFC (LBG) | Shenmao | PF606-P | SAC305 | Type 4
 | LCFC (TBG) | Senju, Alpha |  | SAC305 | Type 4
Solder Paste

## Slide 6
No | Customer | Please list the Screen Print Machine used | 
 |  | Vendor | Model
 | Quanta SH | Panasonic | KXF-1G4C
 | Quanta CQ (F1) | Dek | Horizon O3iX
 | LCFC | Hitachi | HS-710
Screen Print Machine

## Slide 7
No |  | Pressure | Print Speed | Separation speed
 | Quanta SH | 60 x 10-2 N | 80 mm/s | 5.0 mm/s
 | Quanta CQ | 16 kg | 60 mm/s (NPI), 100 mm/s (HVM) | 20mm/s
 | Wistron KS |  | 100 mm/s | 
 | Compal KS | 15 kg | 80 mm /s | 1.0 mm/s
 | LCFC | 2.4 x 0.1 Mp | 60mm / s (NPI), >100mm / s (HVM) | 2.5 mm/s (40% - 180 %)
Printing Parameters

## Slide 8: SPI

## Slide 9: SPI Machine
No | Customer | Please list the AOI Machine used | 
 |  | Vendor | Model (Control)
 | Quanta SH | Saki | 
 | Quanta CQ (F1) | Cyber Optic | SE50 (-60% - +90%)
 | Wistron KS | KY | (40% - 170%)
 | LCFC | KY | 8030 XDL

## Slide 10: Placement

## Slide 11
No | Customer | Please list the BGA Placement Machine used | 
 |  | Vendor | Model
 | Quanta SH | Panasonic | KXF-E64C
 | Quanta CQ | Panasonic | NPM
 | Compal KS (Dell) | Panasonic | KXF-E (DT 401-F)
 | LCFC | Panasonic | 
BGA Placement Machine

## Slide 12: Reflow

## Slide 13
No | Customer | Q1: Reflow Machine's |  | Q2: N2 reflow? | Q3: O2 ppm level
 |  | Brand | Model |  | 
 | Quanta CQ | Rehm | 13 zones | Yes | <1000ppm
 | Wistron CD | Honey Well | 1900 | Yes | <3000ppm
 | Compal KS (Dell) | BTU | Pyramax | Yes | 
 | LCFC | Rehm |  | Yes | 449 ppm
Reflow Machine, N2 and O2 ppm Level

## Slide 14
No | Customer | With Pallet / Carrier? |  | 
 |  | Yes / No | Product specific / generic pallet? | What material used for Pallet fabrication?
 | Quanta SH | Yes | Specific, no clamp | Aluminum
 | Quanta CQ | Yes | Universal during NPI | Aluminum
 | Compal KS (Dell) | Yes | Specific, no clamp | Aluminum
 | LCFC | Yes | Universal | Aluminum
Reflow Pallet and Material

## Slide 15
No | Customer | Belt Speed (cm/minute)
 | Quanta CQ | 1400 mm / min
 | Wistron KS | 100cm / min
 | Compal KS (Dell) | 105 cm / min
 | LCFC | 1350 mm / min
Belt Speed

## Slide 16
No | Customer | Peak temperature (°C) | TAL | Soak Time | Max Rising Slope | Max Falling Slope
 | Quanta CQ | 230 – 250 | 60 – 80 sec | 155 – 185 (60 – 120 sec) | 0 – 3.0 | 1 – 3.0
 | Wistron CD | 235 – 250 | 40 – 90 sec |  | <3.0 | <-3.0
 | Wistron KS | 235 – 250 |  |  |  | 
Reflow Profile Parameters

## Slide 17: Rework