## Slide 1: APAC Client ODM - BGA Adhesive Usage Information
Updated as of WW16’17
Ack: CMEE Team for collecting this information (SA Moy, Harry Yu, Jagadeesh Radhakrishnan)
Customer Sensitive Information – Never Forward, Never Share

## Slide 2: BGA Adhesive Usage
BGA Adhesive |  |  |  |  |  |  |  |  |  |  |  | 
 |  | Inventec CQ | Quanta CQ | Quanta SH | Compal CQ | Compal KS | Wistron KS | LCFC / Lenovo | Pega SZ | MSFT / JDM1 | MSI KS | Summary
1 | Are you currently using adhestive for Intel BGA in HVM? | Yes. | Yes. | Yes. | Yes | yes | Yes | 100% underfill for all projects request by customer | Yes | Not for Intel CPU, because pass reliability test w/o glue. | Yes | Except for Microsoft, all customers are using corner glue (Red glue or UV glue), LCFC/Lenovo are also using underfill.
2 | What's the reason you apply adhesive for Intel BGA? | Enhancing BGA balls' solderability & reliability | Prevent solder crack | Prevent solder crack | Customer request (Major customer Acer) | reliability | crack resistance | Reliability | Reliability |  | Increase strength | Reliability, prevent solder crack
3 | What are you using (Example: Corner Glue, Corner dot, underfill, underfilm, corner fill)? | corner glue. | Corner Glue | Corner Glue | Corner Glue | Plant 3: Corner Glue, Plant 4: Underfill | Corner Glue / Underfill | Underfill | UV coner bond |  | Corner Glue, cover until 6th balls. | Corner glue is predominantly used
4 | What's the vendor name and model of the adhesive material you are using? | Loctite 3619 | Loctite 3609 | Loctite 3609, UV glue (EICT) | UV (Vendor: U-BOND; Model: UB-4305) | Plant 3: Loctite 3705 (UV Glue), Plant 4: TBD….. | Corner Glue dot: Panasonic ADE480D-1 Underfill:ASEC-AS3910 | ACES, COOTEK, TaiLiDe | 視域:UV649/信友:3329/DYMAX 9-20558 /Loctite 3705 |  | Vendor : ZhongYu Model: ZY-303 UV cure | 
5 | Where in the board manufacturing process is the adhesive applied (Ex. Before SMT (or) After SMT/Before Functional Test (or) After SMT/After Functional Test)? | After SMT / Before Functional Test | After SMT/Before Functional Test | After SMT/Before ICT Test | After SMT/Before ICT or ATE test | Plant 3: After reflow, before ICT, Plant 4: After ICT | After SMT / Before Functional Test | After function test (ATE test still on for most project unless test coverage very low) | After SMT/Before Functional Test |  | After SMT, passing AOI, Glue --> Routing --> ICT | Surprisingly, almost all customer applying adhesive after SMT, but before ICT test, to prevent solder crack during the test. LCFC applies underfill after test because underfill hard to rework
6 | Is the adhesive reworkable? | Yes. | Yes. | Yes. | Yes | Plant 3: Yes, Plant 4: difficult | Reworkable | Yes | Yes |  | Yes | Yes, but Compal said the underfill is hard to rework
7 | Is the adhesive applied in-line or off-line process? | in-line | In line | In line | in-line | on line | In-line | in line | in-line |  | In-line | all in line
This information was capture during the Cannon Lake Platform Intro tour. These 10 target customers are focused on laptop & 2-in-1 manufacturing, so this Q&A is more toward to this segment.
Update as of April 2017. Clarification from Lenovo: For BGA adhesives they don’t use a full underfill, instead they use “corner fill” (Loctite 3910 adhesive), which covers a min of 5 solderballs in all 4 corners. It could be applied at any of their key ODM sites: Wistron, Quanta & Compal.

## Slide 3: Additional Info per Jagadeesh
I had looked at teardowns of Intel and non-Intel based tablets (back when we were still focused on Tablets). At that time, I noticed that all SoCs (Intel and non-Intel) had corner glue or underfill. So, I would safely say adhesives are common in laptop / 2-in-1 / tablets / cellphones, and adhesives are less prevalent in DT and servers. Cell phones tend to have full underfill.
Additional Info per SA Moy
For tablet, I think it is much more sensitive on mobility (drop test performance). Moreover, if our future is also focusing on LTS process, solder joint protection with using adhesive is a key. In this case, we also need to remind package platform guys that to consider keep out zone for adhesive (corner glue). FYI…. During LTS sharing, a customer even asking us what type of adhesive that Intel recommended.