## Slide 1: KBL-G x-ray exposure customer situation
Harry Yu

## Slide 2: Known customers list and build schedule
OEM | ODM | Project name | Build schedule
Dell | Compal KS | La Ferrari | Next Pilot build 1/24 RTS (Ready To Ship) date 3/29
HP | Quanta CQ | X35A | MV build (200~400Pcs) at 2/24 HVM target end of March
Intel | Pegatron SZ | NUC-3 | 

## Slide 3: Customer X-ray machine survey
KBL-G customer
Quanta CQ said their X-ray machine (Dage XD7600NT) have x-ray source at bottom of the machine. If put BGA up, there are at least a metal table and PCB block in between; Need X-ray machine expert to double confirm.
Customer | Segment | X-Ray Machine Brand and Model | Tube voltage Typical | Tube power Typical | Typical scan time | Working distance (typical)
Compal | Client | Dage XD6500 | MAX:160kv Normal: 100KV | Max:3w | 35s | Not able to provide
Inventec | Client | SEC and X-eye SF160 | 160kVP | 32W | 1.5min/pcs | 0.3m
Pegatron | Client | Brand：YXLON Model:Cougar SMT | 100KV | 10ua | Not able to define(depends on X-Ray locations and qty). | Not able to define
ODM4 (Pegatron) | Client | PHOENIX; model: ANALYSER 160 | 160kv | 20w | No standard inspection time, depends on on FA purpose or FAI validation. | 310mm
Quanta | Client | Dage XD7600NT | 90KV | 1.2W | /(per sample size) | 90mm
Wistron | Client | Brand: Dage Model: XD7500NT | Max voltage: 160KV Normal usage: 80kv~110kv | Max power: 3w Normal usage: 1.0~1.5W | <1min | Not allow anybody within 1m range except X-Ray machine operator.
Inventec | Server | Vitrox V810xxl S2i | 130 kV | 30mA | 8inch²/s | 2.5cm for the above and 8 cm for below
Quanta | Server | Agilent 5DX 5000 | 160KV | 16W | 120S | 30cm
Quanta | Server | ViTrox V810 | 130KV | 26W | 100S | 30cm

## Slide 4: Customer x-ray usage model (Compal/Dell La Ferrari)
  Debug: When debug engineer suspect SJ failure on BGA, it will be x-ray’d to double confirm
  Repair: Every board been through BGA replacement will do x-ray to confirm sold joint quality
  FAI (First Article Inspection): 1. Every time when new build start, 1 board will send to X-ray per FAI rule. 2. Configure change: Every time when board configure change, 1 board will send to x-ray as part of FAI

## Slide 5: Customer x-ray usage model (Quanta/HP X35A)
  Debug: When debug engineer suspect SJ failure on BGA, it will be x-ray’d to double confirm
  Repair: Every board been through BGA replacement should do x-ray inspection to confirm sold joint quality
  FAI (First Article Inspection): The first board (post reflow) of every work order will send to x-ray inspection
  Sampling check: Random pick 1 board/day send for x-ray inspection
  ICT/ATE open/short issue: Every board need send to X-ray inspection to double confirm whether the open/short caused by SJ issue or not

## Slide 6: Customer x-ray usage model (Intel/ODM4 NUC-3)
  FAI while a new WO;
  FA tool if any defects may relevant to BGA parts;
  Validation tool for any possible process risk

## Slide 7: Compal KS X-Ray Process Characterization Results
Date | Run # | Tool | PCB Design | Inspection State | Filter | Exposure Time (min) | Power Level | Dosimeter Accuracy | Measured Value (mGy) | Measured Value (Rd) | X-Ray Limit, Pass / Fail
7-Mar-18 | 1 | Dage XD6500 | La Ferrari | Manual | No Filter / No Fixture | 10 | 100KV/2.1W | ±5.5% | 42.47 | 4.25 | Pass
7-Mar-18 | 2 | Dage XD6500 | La Ferrari | Manual | Compal Fixture (w Filter) | 10 | 100KV/2.1W | ±5.5% | 3.79 | 0.38 | Pass
7-Mar-18 | 3 | Dage XD6500 | La Ferrari | Manual | On unit Filter | 10 | 100KV/2.1W | ±5.5% | 7.49 | 0.75 | Pass
7-Mar-18 | 4 | Dage XD6500 | La Ferrari | Manual dynamic, simulate normal production | Compal Fixture (w Filter) | 7'03" | 100KV/2.1W | ±5.5% | 6.93 | 0.69 | Pass
7-Mar-18 | 5 | Dage XD6500 | La Ferrari | Manual dynamic, simulate normal production | On unit Filter | 6'48" | 100KV/2.1W | ±5.5% | 16.74 | 1.67 | Pass
Harry worked with Compal KS to characterize their X-Ray process on KBL G42 with a DOE & Dosimeters. See the table below for the details.
In Summary, All the legs passed the <12 Rad criteria
Compal X-ray machine is Dage XD6500, a relative older machine compare to Intel's Dage XD 7500
Compal's normal voltage setting is 100KV, and the machine maxim power setting is 2.1W
Compal build a fixture with a 2 cm (20,000um) copper filter under HBM die to protect the HBM.
There are total 5 DOE legs:
  Leg1: No filter/No fixture, focus on HBM die for 10min. For the FOV and Pixel resolution, Compal didn’t find the setting on their machine, so we just take picture to show how many balls we can see on the monitor
  Leg2: Use Compal fixture, focus on HBM die for 10min
  Leg3: Use x-ray filter, focus on HBM die for 10min
  Leg4: Use Compal fixture, simulate the normal product inspect (Zoom in/Zoom out, move around to inspect all the BGAs, tilt to inspect solder ball opens etc). Total used 7’03”.
  Leg5: Use x-ray filter, simulate the normal product inspect. Total used 6’48”.
For leg 4 and leg5, although the time is shorter than leg 2 and Leg3, the number is higher than leg 2 and 3. Hypothesis the reason is that Compal is zooming in more often, to inspect the details up close.

## Slide 8: Intel NUC X-Ray Process Characterization Results
Harry worked with Intel NUC to characterize their X-Ray process on KBL G42 with a DOE & Dosimeters. See the table below for the details.
In Summary, All the legs passed the threshold

## Slide 9: Quanta CQ X-Ray Process Characterization Results
Harry worked with Quanta CQ to characterize their X-Ray process on KBL G42 with a DOE & Dosimeters. See the table below for the details.
Quanta CQ have the same Dage machine in our CPTD. The Leg 1 and Leg 2 have similar data as we got in our CPTD line:
  Leg1: 3min without filter, Intel: 3rad, Quanta CQ: 2.71 rad.
  Leg2: 5min without filter, Intel: 9rad, Quanta CQ: 8.21 rad
  Leg3: Simulate production scan w/o filter, board zoom in/out and move around to check different component. Quanta used 16’46” finished 1 board scan and the x-ray dosage exceed the threshold.
  Leg4 and 5: By mistake, they put the x-ray filter on top of the memory die (BGA between filter and x-ray source) instead of bottom of the BGA, thus the number is very high.

## Slide 10: AR update
  Confirm the machine info we already have: See previous page
  Ask for the distance from the x-ray source and object: See previous page
  Ask for the min & max typical exposure times under x-ray: Typically <5min in manual scan
  Ask for what side of the board is up or down during x-ray: Typically put BGA side up during manual scan
  Ask if they run 100% of boards through x-ray or just a sampling? If sampling, what is the sampling rate? : Just sampling, Sampling rate various depends on different customer process
  Ask what tool do they run in HVM: Client customers are using off line x-ray machine to do manual inspection. Server customer will use online AXI check