## Slide 1: 2021 MTL Customers CRD Summary Report
Rev1.0, CQ&R CMEE Team, 2021Q3
Stop
Customers confidential information under NDA, Intel internal use only

## Slide 2: General SMT Line Layout
Solder Paste Inspection (SPI)
Pre-Reflow Automated Optical Inspection (AOI) - Optional
Post-Reflow Automated Optical Inspection (AOI)

## Slide 3: Objectives
Data Collected From 10 ODM Customers/Sites
  Compal (KunSan – Build for Dell/HP, ChengDu – Build for Dell, ChongQing – Build for Acer)
  HuaQin (Build for HuaWei/Asus/Lenovo/Samsung)
  Inventec ChongQing (Build for HP/Asus)
  LCFC (Build for Lenovo)
  MSI KunSan (Own Brand)
  Pegatron (ChongQing – Build for Asus)
  Quanta (ChongQing – Build for HP)
  Wistron TaiWan (Build for Lenovo)
Share Findings From CMEE Mobile Industry Data Collection (MTL Platform Customer Survey)

## Slide 4: Highlights
Due to most customers aren’t in LTS HVM yet, thus for a lot of LTS related questions customer answered using SAC experience
T4 still the major paste customer is using. And step stencil is widely accepted in the industry 
Only 3/10 customers have thermal cure adhesive process. Anticipate high customer impact if must use thermal cure process 
Thunderbolt and SD WIFI module are the most common Intel branded component used by customer 
Customers are worrying about MTL M max temp 200C because they afraid during rework process the component body temp will over the limit 

## Slide 5: Solder Paste Printing

## Slide 6: Solder Paste Printing (1 Of 6)
Have you had any prior experience printing paste 0.37mm pitch BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | No, min 0.4mm | No | Yes | Yes 0.35mm pitch CSP
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Lenovo: No ThinkPad: Yes,0.35mm | No | Yes | No, min 0.4mm | Yes, 0.35mm
Which Stencil tension type & values are you using for 0.37mm pitch BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
50N | 32-35N | >35N | 45N~50N | >=30N
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
N/A | Not using 0.37mm BGA now | 38~42N | 30~50N | 32~38N
Half of the customer have small pitch (<0.4mm) print experience

## Slide 7: Solder Paste Printing (2 Of 6)
List top 3 LTS pastes and percentage of each type planned to use in your production line for MTL-M |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | Nihon B37 | Eunow DW1000 (still testing) | NA, current testing Eunow, ShenMao and Koki
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Lenovo: 金讯EcoLM-C15-GL，Bi 49%-53%. (100%) ThinkPad: Senju L28-N143HF (100%) | NA | Current testing: 1.Eunow DW1000 2.YunNanTin YT-AB02 (57% Bi) | Shenmao PF735-PQ10; Aojiang HN-302; Compo LF143S-PF. | Shenmao: PF735-PQ10-10 Sn-48Bi-Ag-X (Intel) Senju: L29-145HF Sn-58Bi-Sb-Ni (Evaluating) Senju: L28 -N143HF Sn-35Bi-0.5Cu-0.03Ni (Lenovo)
Few customers using LTS paste outside Intel recommendation list. Most still near eutectic, few of them are none-eutectic
* Red means the paste is not in our recommendation list
Notes: Double confirm Think pad LTS paste

## Slide 8: Solder Paste Printing (3 Of 6)
For MTL-M BGA package with 0.37 mm pitch, what is solder paste mesh size planned to be used? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
T4 | T4 | T4 | T5 | T4.5 or T5
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
T5 | NA | T4 | T4 | T4
For 0.37mm BGA pitch, will you use a single stencil thickness or a stepped stencil? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Use Step stencil | Most situation use step stencil (for connectors) | Few situation use step stencil | Few situation use stepped stencil | Most situation use step stencil
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Use step stencil | Yes, 100% use step stencil | Most situation use step stencil | Few situation use stepped stencil | Not use step stencil
T4 is still the major paste type;
More and more customer now using stepped stencil then before

## Slide 9: Solder Paste Printing (4 Of 6)
If a single stencil thickness (mm or mils) is used for 0.37mm BGA pitch, what is your thickness preference? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
3mil | 3mil | 3mil | 3 mil | 3mil
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
0.06mm (~2.5mil) | NA | 3mil | 0.06mm (~2.5mil) | 3mil
When using step down stencils, what is max print (squeegee) speed (mm/sec)? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
200mm/s | 100mm/s | 80mm/s | 80 mm/s | 120mm/s
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
150mm/s | 70 ±20mm/s | 80～120mm/s | 120mm/s | Same as no step
When using step down stencils, what is print (squeegee) pressure (kg)? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
8kg | 0.5kg per 25mm squeegee length | 7kg | No answer | 11Kg
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
0.26Mpa(Hitachi) | 12±4kg | 8～12kg | 10Kg | Same as no step
3mil stencil still most commonly used for <= 0.4mm BGA

## Slide 10: Solder Paste Printing (5 Of 6)
For 0.37mm pitch BGA, what is the smallest AR (Area Ratio) capable in HVM |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
0.69 | 0.7 | 0.62~0.7 | 0.625 | 0.66
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
0.7 | NA | 0.7 | > 0.7 | 0.68
Is nanocoat technology used on stencil for 0.37 mm pitch BGA |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Will consider it | Not using now | Will consider it | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | NA | Fine Grain always, and some projects use nanocoat | Yes | Yes
How many strokes for kneading (per print direction) when a new paste is applied onto the stencil? Please also state if different for LTS vs. SAC. |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
2 | 4 | 3~5 | 6 | 2
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | 2 | 2 | No | 1~3

## Slide 11: Solder Paste Printing (6 Of 6)
What is the auto cleaning frequency / setting of the stencil (how many print strokes before stencil is cleaned)? Please also state if different for LTS vs. SAC. |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
8 | 6 | 6~10 | 4 | 6
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
15 | 4 | 3～6 | 6 | Min: 1~3
Please describe under what conditions boards are either washed / cleaned manually (IPA) versus Ultrasonically? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Manual | Manual | Manual | Manual | Manual (IPA)
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Manual IPA | Manual first, then use equipment | Manual | Ultrasonic | Special equipment
Most customers still use manual clean process for mis-printed boards

## Slide 12: Solder Paste Inspection (SPI)

## Slide 13: Solder Paste Inspection (1 of 2)
What are your SPI volume control limits (+/- %) for 0.37 mm pitch BGA |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
50% - 150% | 70% - 165% | 80% - 140%（LTS) | 40% - 160% | 60% - 160%
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
50% - 140% | NA | 50% - 180% | 50% - 150% | Follow customers
For SPI volume control limits with 0.37mm pitch BGA, what is percentage of defects? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | NA | NA | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
NA | NA | NA | NA | NA
Customers still follow their standard SPI control limits even for small pitch BGA similar to prior survey

## Slide 14: Solder Paste Inspection (2 of 2)
What are your SPI X (um) and Y (um) offset limits for 0.37 mm pitch BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
20% | 50% | 30um | 33 um | 70um
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
50um | NA | 40% | 100um | Follow customers
What is the SPI tool threshold setting values (um) used in the algorithm? [FYI: The threshold value is the minimum height above which the volume is measured. The threshold value is measured from either the Cu or from the Soldermask (tool decides based on the pitch)]. |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
35um | NA | NA | 4um | 30um
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
50um | Confidential | NA | NA | Follow customer’s request

## Slide 15: Pick and Placement (PnP) Machine

## Slide 16: Pick and Placement (PnP) Machine (1 Of 1)
State BGA Placement Force in Newtons when Intel MTL-M 0.37mm pitch BGA is placed? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
2.5N | 2.5N | 2.5N | 2.5N | 2.5N
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
2.5N | NA | NA, Fuji NXT | 2.5N | 2.5N
Under what conditions do you decide to use a whole process pallet? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Current no such requirement | 1. No breakout process edge 2. PCB T<0.8mm | Current no such requirement | PCB T<0.8mm | PCB T<0.6mm
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
1. No breakout process edge 2. PCB T<0.6mm | Current no such requirement | PCB T<0.8mm | PCB T<0.7mm | Depends on product size, weight and PCB thickness
Customers use whole process pallet in 2 conditions:
There is no breakout process edge designed for the PCB
PCB T < 0.6~0.8mm

## Slide 17: Reflow Convection Oven

## Slide 18: Reflow Convection Oven (1 of 3)
What will be your Peak Temperature Range for LTS BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
165~175C | NA | 185~200C | 165 - 180C | 170C - 185C
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Lenovo:180+/-5C ThinkPad:190-195C | NA | 160-180C | Shenmao, 155-185C; Aojiang HN-302, 160-180C; Compo LF143S-PF, 180-200C. | Depends on paste PF735-PQ10-10 165 - 175C L28 -N143HF <190C
The highest peak reflow of LTS process <=200C

## Slide 19: Reflow Convection Oven (2 of 3)
Do you measure the cooling slope for reflow profile for SAC? If yes, what is the criteria for passing? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
-4~-1C/S | -3~-1C/S | -3~-1C/S | -3~-1C/S | -3~-1C/S
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
-3~-1C/S | -3~-1C/S | -3~-1C/S | NA | Depends on product
Do you measure the cooling slope for reflow profile for LTS? If yes, what is the criteria for passing? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | -3~-1C/S | -3~-1C/S | -3~-1C/S
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Lenovo:-4~-1C/S ThinkPad -3~-1C/S | NA | -5~-1C/S | Shenmao, -6~-1C/s; Aojiang HN-302, -8~-3C/s; Compo LF143S-PF, ≤-4C/s. | -3~-1C/S, <115C out of reflow oven
- If yes, how do you calculate the cooling slope for LTS? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | NA | Max slope over 20 seconds down to 120C | Max slope over 60 seconds down to 110C
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Max slope over 65 seconds down to 100C | NA | NA | NA | NA

## Slide 20: Reflow Convection Oven (3 of 3)
What changes will be made to reflow oven to accommodate an LTS reflow profile? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | Change heating zone temp setting and belt speed | Change heating zone temp setting and belt speed | Change heating zone temp setting and belt speed
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Change heating zone temp setting | NA | Change heating zone temp setting and belt speed | NA | Change heating zone temp setting
Do you plan to follow all of the Intel MAS for LTS reflow parameters? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | NA | Yes | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No, we will follow paste vendor suggestion | NA | Yes | Yes | Yes, will consider Intel MAS and paste vendor suggestion
What is the Belt Speed (cm/min) used for an LTS profile? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | 90cm/min | 120 cm/min | 125 cm/min
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
140cm/min | NA | 100cm/min | NA | Depends on product

## Slide 21: Adhesive SJR (Solder Joint Reliability)

## Slide 22: Adhesive SJR (1 of 5)
How do you decide whether to use board level adhesives on LTS? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Always use UV corner glue for big BGAs | Always use UV corner glue for big BGAs | Always use UV corner glue for big BGAs (CPU, GPU, SSD) | Use corner glue all the time | Follow customer requirement + drop test result
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Always use underfill for > 10x10mm BGAs (CPU/GPU/RAM/PCH) | NA | NA | Always use corner glue for key components. Current evaluating SJEM process | CPU+Customer requirement+test fail location+high stress area
Do you follow Intel's MAS dispense & KOZ recommendations for Client Mobile Products with regards to adhesive material? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | Yes | Yes | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | Yes | Yes | Yes | Depends on customer requirement
What adhesive brand and model do you use for LTS? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | UV glue | LOCTITE 3705 (UV) | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
ASEC 3917 Syscotech(新懿) AS3109A7 (Corner Underfill) | NA | SeaYu(信友) UV3329 (UV) | NA | Loctite 1172A (Intel required underfill)

## Slide 23: Adhesive SJR (2 of 5)
Do you apply adhesives to other Intel branded components (Eg: PMIC, Thunderbolt, Wifi, Clover Falls, etc...) on motherboards manufactured with LTS pastes? (Answer "NA" if not using other Intel branded components) |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | Depends on dispense spacing | No | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes, PCH | Yes, PCH | Yes, PCH | Yes, PCH | No
Do you apply adhesives to other non-Intel BOM components (Eg: Memory CSP, Connectors, etc...) on motherboards manufactured with LTS pastes? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | Yes, Memory | No | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes, GPU/Memory | No | Yes, GPU | Yes | Yes, GPU, memory connector, WLAN connector)
CPU, PCH, GPU, Memory are the most common components that customers apply adhesive onto

## Slide 24: Adhesive SJR (3 of 5)
Do you have HVM thermal cure glue process capability in your factory? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | No | No | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | No | No | No | Yes
- If not, what would be the impact to setup thermal cure glue process in future? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Equipment investment, Adhesive Qualification, No enough factory floor space | NA | Equipment investment, Adhesive Qualification, Line reconfig | NA | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Equipment investment, Line reconfig | Unlikely | NA | Line reconfig, Unlikely to implement because heat cure will cause PCBA deformation | NA
Only 3/10 customers have thermal cure adhesive process in their factories. Unlikely implement thermal cure process w/o big impact

## Slide 25: Adhesive SJR (4 of 5)
Do you have HVM underfill/corner fill process capability in your factory? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | No | No | Yes | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | No | No | No | Yes
- If not, what would be the impact to setup underfill/corner fill process in future? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Equipment investment, Adhesive Qualification, No enough factory floor space | NA | Equipment investment, Adhesive Qualification, Line reconfig | NA | Equipment investment, Line reconfig
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
NA | Unlikely | NA | Line reconfig, Unlikely to implement because heat cure will cause PCBA deformation | NA
Only 3/10 customers have underfill/corner fill process in their factories, because they build for Lenovo

## Slide 26: Adhesive SJR (5 of 5)
Do you apply adhesive on BGAs right after SMT/before any test? If yes, what is the reason? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes, easy to apply glue before depanel | Yes, to prevent SJ crack | NA | No | Yes, to prevent SJ crack
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | Yes, easy to apply glue before depanel | Yes | Yes | No
Do you have Pre-Reflow In-Line adhesive dispense capabilities, to hold select SMT parts from falling off the board on the 2nd Pass through SMT? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | Yes | Yes | No | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | Yes | No | No | Yes
2 reasons customer apply adhesives right after reflow:
Easy to process before the board was de-panel-ed
Prevent solder crack on the following mfg process

## Slide 27: X-Ray FA Capability

## Slide 28: X-Ray FA Capability (1 of 1)
State Xray (Failure Analysis) Supplier Name, Model# and Year of Manufacture, used for Intel BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Nordson-XD7500VR | Dage -XD7500/2007Y | NA | phoenix xlaminer MXCN000619-332618 March 2019 | SEC X-eye SF160 2013/04/25
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Nordson/Dage-Quadra6-Year2018 | Old machine, 15 years ago | YXLON Y.Cougar.SMT 2014/12 | Nordson/Dage-Quadra7 | Dage & TRI

## Slide 29: Rework

## Slide 30: Rework (1 of 5)
What is the Rework Tool used for LTS BGA formulation? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
QUICK EA-H15 | QUICK EA-H15 | QUICK EA-A10 | Ersa HR 600-2 | 业欧 PFT-950/业欧 TP-500
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Ersa HR 600-2 | NA | Hipo Tech RD500-Ⅲ; HBR-RD500S | No answer | SRT2200i
Does the Rework tool use Convection Air or Infrared Air for heating package/board during reflow? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
IR | IR | Both | Convection Air | Top: Convection Air + Bottom IR
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
IR | NA | Convection air | IR | Convection air
What tool is used for site dress of pad site after component removal for 0.37 mm pitch Intel BGA package? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
4C houseshoe iron tip | 4C houseshoe iron tip | Iron tip | 4C houseshoe iron tip | Auto scavenger tool
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
4C houseshoe iron tip | NA | 4C houseshoe iron tip | No answer | Iron tip

## Slide 31: Rework (2 Of 5)
What is the iron tip temperature setting for site dressing of LTS BGA rework? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
420C (SAC) | 370-390C (SAC) | 380C (SAC) | 250C | 250C
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
390±5C | NA | 250C | NA | 350C
When is paste or Flux used for Intel SOC for LTS BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Print paste to BGA ball + apply flux to PCB pad | Paste | <0.4mm, use flux, >= 0.4mm, use paste | Paste | Paste
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Paste | NA | <0.35mm, use flux, >= 0.35mm, use paste | <0.4mm, use flux, >= 0.4mm, use paste | Paste
Most customers still capable to print paste for BGA pitch = 0.4mm

## Slide 32: Rework (3 Of 5)
Please state LTS Paste Vendor Name and Formulation name for BGA rework? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
YunNan Tin YW9-3005-98CY04 (SAC) | YunNan Tin YW9-3005-98CY04 (SAC) | Nihon B37 | N/A (Current is testing Eunow and Shenmao) | N/A (Current testing Eunow, Shenmao and Koki)
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Lenovo: 金讯EcoLM-C15(100%) ThinkPad: Senju L28-N143 (100%) | NA | NA | NA | Same as SMT paste
Please state LTS Flux Vendor Name and Formulation name for BGA rework? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
AIMSOLDERPASTE NC254 (SAC) | AIMSOLDERPASTE NC254 (SAC) | NA | NA | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
AMTECH-559 | NA | Eunow PASTE FLUX 100G/B07 (SAC?) | NA | Same as SMT paste

## Slide 33: Rework (4 of 5)
Do you plan to follow all of the Intel MAS for LTS rework parameters? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | Yes | Yes | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | NA | Yes | Yes | Will follow paste vendor recommendation and Intel MAS
Cycle Time (average) in mins to replace/remove LTS BGA? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
30min | 20-25min | 25min | 20min | 30min
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
25min | NA | 23min | 25min | 30min
Have you had success reworking with solder pastes at your facility for BGAs >0.35mm and <=0.4mm pitch or had any prior experience working with BGAs >0.35mm and <=0.4mm pitch? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | Yes | No | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | Yes | Yes | Yes, success rate 70%~80%. 0.4mm (~800 pins) | Yes

## Slide 34: Rework(5 Of 5)
If N2 is needed for rework, what is the factory impact of installing it? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Not likely | Need new equipment | Not likely | Need new equipment | Need new equipment, not likely now
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
NA | NA | NA | NA | NA
Which flux type do you prefer for reworking full stack LTS BGAs with >0.35mm and <=0.4mm pitch? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
RF | RF | Use paste instead of flux | RMA | NA
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
RF | NA | RMA | NA | RF
Only very few customers are capable for N2 rework (Pls refer to ADL CRD)

## Slide 35: Large EMI Shields ( > 40 x 40 mm)

## Slide 36: Large EMI Shields(1 of 1)
For an LTS process, do you utilize any solder additive process for the EMI shield (>40 x 40mm size) in reflow to increase mechanical stability? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Step stencil | NA | Step stencil, enlarged stencil apetures, top hat on reflow pallet | Step stencil | Step stencil, small solder chip additive
LCFC | MSI | Pega CQ | Pega SZ (JDM1 + Intel SPG & NSG) | Wistron
NA | Step stencil | Step stencil and/or enlarged stencil apetures | NA | NA
Step stencil is the most common method for solder paste additive

## Slide 37: Bare PCB (Printed Circuit Board)

## Slide 38: Bare PCB (1 Of 1)
Is your entire motherboard to be built with LTS paste? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Will consider it | NA | Yes | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | NA | Yes | Bottom SAC, Top LTS | Yes
Are there plans, or a desire, to surface mounting the MTL-M (having LTS ball) with SAC pastes (reverse hybrid)? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | No | No | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | NA | No | NA | No currently, If Intel has the data pls share

## Slide 39: LTS (Low Temperature Solder)

## Slide 40: Low Temperature Solder (1 of 3)
What are your LTS preferred paste formulation? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
NA | NA | Hypoeutectic Bi% (35-40%) | Near Eutectic Bi% (58%) | Near Eutectic Bi% (58%)
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Near Eutectic Bi% (58%) | NA | Depends, haven't decided yet | Depends, haven't decided yet | Near Eutectic Bi% (58%)
Are you planning to use Intel Branded Components other than MTL-M SOC on your motherboards?(If Yes, please answer the next question) |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | No | Yes | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | Yes | Yes | Yes | NA
- What other Intel branded components are you planning to use on your motherboards? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
WIFI | NA | Thunderbolt, WIFI | WIFI | WIFI
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
PMIC, Thunderbolt, WIFI | WIFI | WIFI | Thunderbolt, WIFI | N/A

## Slide 41: Low Temperature Solder (2 of 3)
What is the maximum board thickness you will surface mount MTL-M BGA onto? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
1.2mm | NA | 1.0mm | 1.0mm | 1.2mm
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
1.2mm | 1.2mm | 1.0mm | 0.7~0.8mm | 1.2mm
Are there any other component suppliers providing full stack LTS BGAs? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | NA | No | No | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | No | No | No | No
Do you have any concerns if the maximum peak reflow temp for LTS, supported in the MTL-M MAS, is 200C? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | NA | Yes | No | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | No | No | No | No
ODM is worrying about the package body temp will over 200 C during rework process. Wistron measurement shows BGA body temp at 202c (peak temp 200C) during LTS rework. Consider some LTS paste will require peak temp up to 220C, Wistron’s preference of MTL M max temp is 230C.

## Slide 42: Low Temperature Solder (3 of 3)
Based on your available data, what is the risk level to implement LTS process on MTL-M product(s)? : Please select one: A. Low and ready. B. Medium and still need to collect some data C. High and limited data available D. Show stopper |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
D. Show stopper | D. Show stopper | B. Medium and still need to collect some data | C. High and limited data available | B. Medium and still need to collect some data
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
A. Low and ready. | C. High and limited data available | B. Medium and still need to collect some data | D. Show stopper | A. Low and ready.
If answer is B, C or D, please provide what data is required to bring risk level down to Low? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
SJO, SJ crack | NA | SJ strength compared to SAC | Dye Pry Humidity Test Corner Drop Test Thermal Shock Test Fragility Shock and Vibration Torture Test I/O connector strength and durability Weighted Vibration Test Weight Drop Test | SMT setting and SJ reliability test
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
During rework the CPU surface temp will > 200C | Component max temp, HT warpage, SJ reliability | Still under test | No answer | NA

## Slide 43: SD WLAN

## Slide 44: SD WLAN (1 of 4)
What is the percentage of your design having the SDWLAN on the opposite side with major BGA (CPU, Gfx etc)? Please provide a rough % number. |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
30~40% | NA, not using SDWLAN | 10% | 10% | 0%
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
0% | 10% | 0% | 20% | Not using SDWLAN
Where is the SDWLAN located in your board design? Please answer: Center, Edge, Corner (Refer to the picture-->) |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Edge | NA | Edge, corner | Corner | Edge, Corner
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Edge | Corner | Edge, corner | Edge, corner | 
In your design, what is the closest distance from board edge/corner to SDWLAN module? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
1mm | NA | >5mm | 1.5mm | 1mm
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
5mm | 5mm | 0.5mm | 20mm | 

## Slide 45: SD WLAN (2 Of 4)
What is the % of your projects are using 3mil stencil and what the % of 4mil stencil for SDWLAN solder down? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
100% 4mil | NA | 100% 4mil (~100um) | 100% 4mil (~100um) | 20% 5mil (~127um), 80% 4mil (~100um)
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Lenovo:80% 4mil，20% 5mil ThinkPad:0.11mm 80% 0.1mm 20% | 90% 4mil | 100% 4mil | 100% 4mil | 
Do you need to have a 3mil stencil thickness recommendation in the Intel MAS? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes | NA | No | Yes | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes | Yes | Yes, we use more and more 3mil stencil, step stencil will impact print quality, we prefer to have 3mil recommendation | No | 
Current 4mil and 5mil stencil still the mainstream for SDWLAN, but big portion of customers are hoping to have 3mil stencil recommendations

## Slide 46: SDWLAN (3 of 4)
Do you scan the SN# of Intel SDWLAN module, and link it with board SN# and save it into your database? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | NA | No | No | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | No | No | No | 
- If yes, can you provide the specific scanner (brand, model) you are using and what is the distance/angle when you scan? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | NA | No | No | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
NA | NA | NA | NA | 
Are you aware of the Intel SDWLAN new land pattern recommendation? To date, how many of your designs had implemented this new land pattern? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
Yes, havn't implement yet | NA | Will implement for all future project | Yes, 70% current design and 100% all future new design | Yes
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Yes, 7% existing projects, 100% for future new projects | Unclear | Yes, 3 projects now. 100% for future projects | Yes | 

## Slide 47: SDWLAN (4 Of 4)
Do you have any suggestions to Intel to further improve the PCB land pattern design? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | NA | No | No | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
No | SDWLAN warpage after reflow causing SJO and SJ short, it is keeping on bothering us | No | Less via hole on the footprint | 
Do you have any suggestions to Intel to further improve the SDWLAN module design aimed to achieve higher SMT yield? |  |  |  | 
Compal CD | Compal CQ | Compal KS | HuaQin | Inventec CQ
No | NA | No | No | No
LCFC | MSI | Pega CQ | Quanta CQ | Wistron
Recommend LCC type package | No | No | IO extend to substrate edge |