## Slide 1: 2023 LNL&ARL Customers CRD Summary Report
Rev2.0, CQ&R CMEE Team, 2023Q2
Stop
Customers confidential information under NDA, Intel internal use only

## Slide 2: General SMT Line Layout
Solder Paste Inspection (SPI)
Pre-Reflow Automated Optical Inspection (AOI) - Optional
Post-Reflow Automated Optical Inspection (AOI)

## Slide 3: Objectives
Data Collected From 10 ODM Customers/Sites
  Compal (KunSan – Build for Dell/HP, ChengDu – Build for Dell, ChongQing – Build for Acer)
  HuaQin (Build for HuaWei/Asus/Lenovo/Samsung)
  Inventec ChongQing (Build for HP/Asus)
  LCFC (Build for Lenovo)
  MSI KunSan (Own Brand)
  Pegatron (Suzhou- Build for Microsoft/ChongQing – Build for Asus)
  Quanta (ChongQing – Build for HP)
Share Findings From CMEE Mobile Industry Data Collection (LNL&ARL Platform Customer Survey)

## Slide 4: Highlights
Only LCFC and Compal KS have paste jetting machine experience. 
Only LCFC and Compal KS have LTS HVM experience. LCFC use full board LTS and Compal KS only use LTS on Intel BGA. SPI machine tolerance varies with ODMs. 
Large EMI shield may cause open after soldering. Clip is a good option. 
5/10 ODMs have experience with IR tool. Only LCFC and MSI have capability of weighted load force during reflow. 
Competitor’s BGA has better yield performance, due to the square shape, thicker substrate, larger pitch. 
Competitor’s BGA also has DSC design, and half ODMs have Liquid Metal experience. 
All ODMs have X-RAY, Cross section, Dye&Pry. 3/10 ODMs have SEM/EDS. 

## Slide 5: Solder Paste Printing & Inspection(SPI)

## Slide 6: Solder Paste Printing & Inspection(SPI)(1 Of 5)
 | Have you had any prior experience printing paste on 0.35mm pitch part such as BGA or SMT connectors? | Is nano coating technology used on stencil for 0.35 mm pitch part such as BGA or SMT connectors? | Do you have experience on step-stencil within the BGA field less than or equal to 0.5 mm? | For BGA with 0.5 mm pitch, what stencil thickness do you prefer?
LCFC | Yes | Yes | Yes | 3 mil
Compal CD | Yes | No, keep print quality by reducing stencil thickness | Yes | 3 mil/4 mil
HuaQin | Yes | Yes | Yes | 3 mil
Inventec CQ | Yes | Yes | Yes | 3 mil
MSI | No | NA | Yes | 4 mil
Pega SZ | Yes | Yes | Yes, 0.35 pitch, step down to 0.07mm(2.75 mil) | 0.4 pitch 0.08mm thickness stencil(3.15 mil) 0.35 pitch 0.07mm stencil(2.75 mil)
Compal KS | Yes | Yes | Yes | 3 mil
Quanta CQ | No | No | No | 3 mil
Pega CQ | Yes | Yes | Yes | 3 mil/4 mil
Compal CQ | Yes | Yes | Yes | 4 mil
Most ODMs have experience on printing paste on 0.35 mm pitch part, nano coating technology and step-stencil.

## Slide 7: Solder Paste Printing & Inspection(SPI)(2 Of 5)
 | Do you have experience on paste jetting machine? | If yes, do you have jetting experience on 225 um pad ? | If Yes, please describe your minimum paste deposit diameter and volume capability. | If Yes, please advice the jetting dispense cycle time | If No, do you have any future plans to evaluate a paste jetting process?
LCFC | Yes | Yes, type 5 solder paste | 3*10^-6 cu.mm | Theoretically, 200 point/second, actually 80 point/second | NA
Compal CD | No | NA | NA | NA | Depends on customer requirement
HuaQin | No | NA | NA | NA | No
Inventec CQ | No | NA | NA | NA | No
MSI | No | NA | NA | NA | No
Pega SZ | No | NA | NA | NA | No
Compal KS | Yes | Yes | 200 um diameter | 10 point/second | NA
Quanta CQ | No | NA | NA | NA | No
Pega CQ | No | NA | NA | NA | No
Compal CQ | No | NA | NA | NA | No
Only LCFC and Compal KS have paste jetting machine experience.

## Slide 8: Solder Paste Printing & Inspection(SPI)(3 Of 5)
 | Can you provide your current SAC solder paste list with percent and usage? | Can you provide your current/future LTS solder paste list with percent and usage? | Do you use LTS for other product except BGA? What paste do you use? What kind of product? | What would be the tolerance limits used on the SPI machine for 0.35 mm pitch part?
LCFC | Shenmao 95% | Senju and Shenmao 90% total | Full board | Volume:70%-170%
Compal CD | YunNan Tin：YW9-3005-98CY04,100% | NA | NA | Volume:50%~180%
HuaQin | ShenMao PF606-P, 73%;Eunow EUP-100F,27% | NA | NA | Volume:60%-150%
Inventec CQ | ShenMao PF606-P tamura LTF-204-93IVT, 50%/50% | NA | NA | Volume:60%-140%
MSI | KOKI S3X58-M406-3,100% | NA | NA | No answer
Pega SZ | Senju M705-S101HF(N4)-S4, 50% ,Eunow EUP-1000HQR: 30% | NA | NA | Volume&Area:50%-150% Height: +2mil, -1mil
Compal KS | Shenmao PF606-P, 50%/ YunNan TinYW9-3005-98CY04, 50% | Nihon B37 100% | No | Volume:60%-160%
Quanta CQ | Shenmao PF606-P,100% | NA | NA | Volume:50%-150%
Pega CQ | YunNan Tin YW9-3005-98US04 100% | No HVM plan, verified Eunow DW1000 and YunNan Tin YT-AB02 | NA | Volume:50%-180%
Compal CQ | Shenmao PF606-P 100% | NA | NA | Volume:50%-150%
Only LCFC and Compal KS have LTS HVM experience. LCFC use full board LTS and Compal KS only use LTS on Intel BGA. SPI machine tolerance varies with ODMs.

## Slide 9: Pick and Placement (PnP) Machine

## Slide 10: Pick and Placement (PnP) Machine (1 Of 1)
 | Have you had any prior experience for placing component 6mil (0.15mm/150um) apart? All type of component either passive, BGA, QFN. | Have you had any prior experience for placing component 8mil (0.2mm/200um) apart? All type of component either passive, BGA, QFN. | Have you had any prior experience for printing/placement/inspection/reflow/rework 008004 inch (0201 metric = 0.25mm x 0.13mm)? What is the challenge? | Do you have the ability to support stacked memory assembly(PoP flux dipping process)?
LCFC | Yes | Yes | Yes, not easy to control print quality, low yield, re-do pad design | Yes
Compal CD | No | Yes | No | No
HuaQin | No | Yes | No | No
Inventec CQ | No | Yes | Yes, high risk on skew, tomb stone | Yes
MSI | No | No | No answer | No
Pega SZ | Yes | Yes | Yes, DOE tried. Printing insufficient, missing, high height, higher volume. Soldering failure open, short, shift. | Yes
Compal KS | No | Yes | No | Yes
Quanta CQ | No | No | Yes, high risk on skew, tomb stone | No
Pega CQ | No | Yes, RLC component has bridge risk if tolerance is too big | Yes, high risk on tomb stone, upside down | Yes
Compal CQ | No | Yes | No, 0201 minimum | Yes
Only LCFC and Pega SZ have experience for placing component 6 mil apart. Half of ODMs have the ability of POP process.

## Slide 11: Large EMI Shields ( > 40 x 40 mm)

## Slide 12: Large EMI Shields ( > 40 x 40 mm)(1 Of 1)
 | Do you have concern on placing/solderdown EMI shield/fence with size of around 110 x 80mm? | Do you have concern on placing/solderdown EMI shield/fence with size of around 180 x 50mm? What is the main concern? | What are the maximum EMI shield/fence size that you have experience solder down?
LCFC | Yes, EMI shield warpage/ deformation leads to open after soldering | Yes, EMI shield warpage/ deformation leads to open after soldering | No answer
Compal CD | Yes, EMI shield warpage/ deformation leads to open after soldering | Yes, EMI shield warpage/ deformation leads to open after soldering | 50mm*50mm
HuaQin | Yes, EMI shield warpage/ deformation leads to open after soldering | No experience. If shield too big, split the whole shield into several small shields then solder down separately. | 150*25*30 maximum size for server
Inventec CQ | Yes, EMI shield warpage/ deformation leads to open after soldering | Yes, EMI shield warpage/ deformation leads to open after soldering | 30mm*40mm
MSI | NA | NA | Use clip only
Pega SZ | Yes. Pick and place machine limitation | Yes. Pick and place machine limitation | 100mm*80mm
Compal KS | No concerns | NA | <100mm x 80mm
Quanta CQ | Yes, equipment limitation and material deformation are the main concern. Can split the whole shield into several small shields then solder down separately. | Yes. Pick and place machine limitation | 60mm*30mm
Pega CQ | NA | NA | 80mm*30mm，if the shield if too big, will divide the big shield to small shielding frames
Compal CQ | NA | NA | Use clip only
Large EMI shield may cause open after soldering. Clip is a good option.

## Slide 13: Rework

## Slide 14: Rework(1 Of 5)
 | What is your HVM tool for BGA rework? | Do you have experience with IR(infrared) tools? | If yes, do you what is the max PCB thickness and max layer count you used with it | What other components other than BGAs do you repair with the IR tool?
LCFC | No answer | No | NA | NA
Compal CD | IR(infrared) tool, supplier：QUICK，type：EA-H15 LF | Yes | 14 layers，1.4mm | Rework WLAN module
HuaQin | ESAR HR600/2 | No | NA | NA
Inventec CQ | Convection Air | No | NA | NA
MSI | Convection Air | No | NA | NA
Pega SZ | Convection Air,崴泰VT-360MII(local supplier) | No | NA | NA
Compal KS | Convection Air/IR(infrared) tool | Yes | 1.4mm , 12 layers | NA
Quanta CQ | IR(infrared) tools，supplier：QUICK，type：EA-H00 | Yes | 1.6mm, 12 layers | NA
Pega CQ | Convection Air，supplier：DIC，type：RD500-III | Yes | 0.6mm(???) , 12 layers | Memory
Compal CQ | IR(infrared) tools，supplier：QUICK，type：EA-H15 | Yes | 1.6mm, 14 layers | NA
5/10 ODMs have experience with IR tool.

## Slide 15: Rework(2 Of 5)
 | Do you have experience with laser tools for BGA rework? | If yes, what is the max PCB thickness and max layer count you used with it | If yes, what is the maxium BGA package size? | What other components other than BGAs do you repair with the laser tool?
LCFC | Yes, but not for rework | 1.6 mm，14 layers | As big as Intel BGA | No
Compal CD | No | NA | NA | NA
HuaQin | No | NA | NA | NA
Inventec CQ | No | NA | NA | NA
MSI | No | NA | NA | NA
Pega SZ | No | NA | NA | NA
Compal KS | No | NA | NA | NA
Quanta CQ | No | NA | NA | NA
Pega CQ | No | NA | NA | NA
Compal CQ | No | NA | NA | NA
Only LCFC has experience with laser tools

## Slide 16: Rework(3 Of 5)
 | Do you have capability printing paste with a mini stencil on <0.4 mm pitch part such as BGA or SMT connectors? | If no, what method do you use?
LCFC | No | Flux only
Compal CD | No | NA
HuaQin | No | Flux only
Inventec CQ | Yes, use both mini stencil and flux-only rework process | Both mini stencil and flux-only rework process
MSI | No | Flux only
Pega SZ | Yes | NA
Compal KS | No | Paste jetting machine
Quanta CQ | No | No answer
Pega CQ | No | Flux-only
Compal CQ | No | Flux-only
Only Inventec CQ and Pega SZ have the capability printing paste on<0.4 mm pitch part. <0.4 mm pitch part

## Slide 17: Rework(4 Of 5)
Only Pega SZ has the capability of rework process for components with limit KOZ (< 0.2mm/200 um). Pega SZ and MSI have N2 rework.
 | Do you have capability of rework process for components with limit KOZ (< 0.2mm/200 um)? | If yes, please describe your process | Do you have the capability to use N2 in their rework area, and if not, what would it take for them to add it to their rework machines?
LCFC | No | NA | No
Compal CD | No | NA | No
HuaQin | No | NA | No
Inventec CQ | No | NA | No
MSI | No | NA | Yes
Pega SZ | Yes, JDM1 line | No answer | Yes
Compal KS | No | NA | No
Quanta CQ | No | NA | No
Pega CQ | No, minimum requirement is 0.8 mm | NA | No
Compal CQ | No | NA | No

## Slide 18: Rework(5 Of 5)
Only LCFC and MSI have capability of weighted load force during reflow.
 | Does your rework equipment have capability of applying continuous load force during reflow ? | If yes to question above, what is min to max load force that can be applied by nozzle during reflow | Does your rework equipment have capability of weighted load force during reflow ? | If yes to question above, what is min to max weight that can be applied with nozzle on top of BGA component
LCFC | No | NA | Yes | No answer
Compal CD | No | NA | No | NA
HuaQin | No | NA | No | NA
Inventec CQ | No | NA | No | NA
MSI | No | NA | Yes | 18 g
Pega SZ | No | NA | No | NA
Compal KS | No | NA | No | NA
Quanta CQ | No | NA | No | NA
Pega CQ | No | NA | No | NA
Compal CQ | No | NA | No | NA

## Slide 19: Failure Mode and SMT Yield

## Slide 20: Failure Mode and SMT Yield(1 Of 4)
NWO is the most common failure mode of ADL-P package in ODM sites. ADL NWO issue in 2022 is the main contributor.
 | In normal production (does not count excursion), what is your common SMT related Time Zero failure rate of Intel Client Processor BGAs ? | What is your major solder joint failure mode of Intel Client Processor BGA( P package) SMT yield loss?
LCFC | 1500-2000 DPM | LTS Hybrid: crack between solder ball and pad, SAC:NWO
Compal CD | <500dppm | Corner bridge, NWO
HuaQin | 2400 DPPM | NWO in long edge
Inventec CQ | ＜500DPM, only SMT | Corner bridge
MSI | <500 DPM | NWO
Pega SZ | <500DPM | Corner bridge and NWO
Compal KS | 1000-2000 DPM | NWO in long edge
Quanta CQ | 3000-4000 DPPM, This is over all failure rate include SMT and functional failure | NWO
Pega CQ | 1000-2000 DPM, only SMT | NWO in long edge
Compal CQ | SMT related failure rate <300DPM, over all failure rate 2000-3000 DPPM | NWO(ADL-P)

## Slide 21: Failure Mode and SMT Yield(2 Of 4)
 | What is your major solder joint failure mode of Intel Client Processor BGA( M package) SMT yield loss? | What is your major solder joint failure mode of Intel Client Processor BGA( Hx package) SMT yield loss? | What is your major solder joint failure mode of Intel Client Processor BGA( N package) SMT yield loss?
LCFC | Hybrid: crack between solder ball and pad, SAC:NWO | Hybrid: crack between solder ball and pad, SAC:NWO | Hybrid: crack between solder ball and pad, SAC:NWO
Compal CD | No experience | Corner bridge, NWO | No experience
HuaQin | Almost no failures | Almost no failures | No experience
Inventec CQ | Corner bridge(???) | Bridge in corner, center | Corner bridge
MSI | No experience | HOP | No experience
Pega SZ | No experience | No experience | No experience
Compal KS | No experience | Corner bridge | No experience
Quanta CQ | Didn't distinguish by different skus | Didn't distinguish by different skus | Didn't distinguish by different skus
Pega CQ | Almost no failures, due to small quantity | No experience | Almost no failures
Compal CQ | No experience. | No experience. | No experience

## Slide 22: Failure Mode and SMT Yield(3 Of 4)
Competitor’s BGA has better yield performance, due to the square shape, thicker substrate, larger pitch. Other companies’ products also have NWO issue.
 | In normal condition (does not count excursion), what is your common SMT related failure rate of other company’s Processor BGAs? | What is your major solder joint failure mode of other company’s Processor BGAs SMT yield loss? | Besides Intel BGA, did you see NWO defect mode on other company’s BGA product | If the answer of above question is ‘Yes’, can you specify which product of other company you saw NWO defect?
LCFC | Better than Intel | LTS: SJ crack, SAC:NWO | Yes | AMD CPU
Compal CD | SBB, Open issue on AMD BGA, less than 300 DPPM | Corner bridge, NWO | No | NA
HuaQin | 1700 DPPM | NWO | Yes | Qualcomm product
Inventec CQ | ＜500DPM, AMD BGA has smaller size, bigger pitch, bigger solder ball, easy to reflow, flat shape(not cry shape) | FR is low, almost no failure | Yes | Nvidia GPU has HOP, NWO issue
MSI | <100DPM | SBB | No | NA
Pega SZ | <500DPM | NWO, SBB | Yes | NVIDIA product
Compal KS | No detail data, Intel has higher Failure Rate, larger Solder ball quantity, smaller pitch | NWO, SBB | Yes | NVIDIA product
Quanta CQ | No detail data, AMD BGA was close to square, thicker, less warpage | No answer | No answer | NA
Pega CQ | <500DPM , AMD BGA was close to square shape, bigger stiffener, bigger pitch, no LCSs | MediaTek has HOP issue | No | NA
Compal CQ | <300 DPPM, similar to Intel | Solder ball shift, SBB | Yes | AMD CPU

## Slide 23: Failure Mode and SMT Yield(4 Of 4)
 | If have to choose between HoP or NWO defect, which one is more difficult to resolve? | If yes, can you specify the reasons? | Can you provide any improvement suggestions to Intel BGA package design to improve SMT yield?
LCFC | HOP | Sometimes HoP related to material issue, difficult to investigate | Adjust pad size(increase pad size), reduce package warpage
Compal CD | NWO | NWO RC may be the material warpage, stencil, solder paste volume. Need to analyze more factors | 1.Increase the stiffener size to reduce HT warpage 2.Control the length less than 50mm. Warpage is smaller if BGA length less than 45 mm*. 3. Square shape has less warpage
HuaQin | NWO | NWO need more precise reflow temp control | Increase the substrate Tg rate, reduce warpage
Inventec CQ | NWO | More factors need to investigate, for example, reflow temp, solder paste volume, component warpage etc | Reduce warpage
MSI | NWO | No answer | Increase substrate thickness, increase stiffener width, reduce substrate size
Pega SZ | NWO | NWO is more difficult to solve, HOP is more difficult to detect | No suggestion
Compal KS | NWO | The package warpage is not easy to control by SMT factory | No suggestion
Quanta CQ | No preference | NA | 1. Increase substrate thickness 2. Close to square, don't be too long* 3.Increase the pitch
Pega CQ | NWO | It is more difficult to control warpage on long edge of rectangle shape package. | 1. Control the coplanarity less than 0.1 mm 2. Reduce the length to 30 mm*
Compal CQ | No preference | NA | Reduce package warpage
Most ODMs prefer to resolve HoP compared with NWO.
*Customer feedback 50 mm is a little bit hard for their PnP machine to handle, Quanta suggest to reduce the length to 48 mm

## Slide 24: DSC Preference

## Slide 25: DSC Preference (1 Of 2)
Competitor’s BGA also has DSC design, and half ODMs have Liquid Metal experience.
 | Besides Intel BGA, does other company’s BGA also have DSC (Die Side Capacitor) design? | Do you currently or have future plan to use Liquid Metal as your Thermal Interface Material (TIM)? | What is the solution you implemented to prevent Thermal module interference with or short to DSCs on Intel RPL Hx and ADL Hx BGA?
LCFC | Yes | On trail production, Gamebook | UV glue on DSCs
Compal CD | Yes | Already Mass Production in CD Galio project | UV glue on DSCs
HuaQin | Yes | No | 1. Milling voids；2.Attach mylar
Inventec CQ | Yes | Yes | Kapton tape on DSCs
MSI | Yes | No | Milling voids
Pega SZ | Yes | No, no information from factory side. | No information from factory side.
Compal KS | Yes | Yes | UV glue on DSCs
Quanta CQ | Yes | Yes | Attach mylar on DSCs
Pega CQ | Yes | No | 1. Milling voids；2.Attach mylar
Compal CQ | Yes | Yes | UV Glue cover the DSC

## Slide 26: DSC Preference (2 Of 2)
 | What is the solution you implemented to prevent Thermal module interference with or short to DSCs on other company’s BGA product? | Do you require Intel to remove DSC design on future BGA processors? If yes, can you specify the reason? | If DSC is a must due to functional requirements, any suggestions to optimize the DSC design to minimize the impact to your thermal module design and assembly?
LCFC | UV glue on DSCs | Yes, reduce cost , simplify process | Smaller size DSC will minimize the impact
Compal CD | UV glue on DSCs | Yes, remove DSC will reduce BGA damage risk and simplify process | Use same size DSCs
HuaQin | 1. Milling voids；2.Attach mylar | Yes, lower cost, reduce BGA damage risk | Die should be 1 mm higher than the DSC
Inventec CQ | Kapton tape on DSCs | No opinion | DSCs should be lower than Stiffener
MSI | Milling voids | Yes, reduce manufacturing cost | Die should be at least 0.5 mm higher than the DSC
Pega SZ | No answer | No information from factory side | No information from factory side
Compal KS | UV glue on DSCs | Yes, simplify process | 1. Concentrate together, don't be too scattered.2. Far away from the die 3. Don't be too high, don't exceed the die.
Quanta CQ | Attach mylar on DSCs | Yes, simplify process | No answer
Pega CQ | 1. Milling voids；2.Attach mylar | Yes, reduce manufacturing cost | Move the DSC to the edge, away from the die
Compal CQ | UV Glue cover the DSC | Yes, simplify process | 1.Simplify DSC types, don't design too many different size 2. Concentrate together, don't be too scattered 3. Far away from the die

## Slide 27: Test & Qualification Requirement

## Slide 28: Test & Qualification Requirement(1 Of 9)
All ODMs conduct thermal cycle test.
 | For new product/project launch, do you conduct PCBA and/or system solder joint reliability test? | If the answer is Yes, do you conduct thermal cycle test? | If the answer is Yes, what is the thermal cycle test condition, sample size and pass/fail criteria
LCFC | Yes | Yes | Follow Lenovo's requirement
Compal CD | Yes | Yes | No answer
HuaQin | Yes | Yes | Test Condition: -40°C-85°C，rate:15°C/min, dwell 10-15 min, 300 circles, mainly based on customer's requirement
Inventec CQ | Yes | Yes | Based on customer requirement
MSI | Yes | Yes, use assembled system | 40℃+90RH,60℃+30RH,12 hours/circle
Pega SZ | Yes | Yes | Customer conduct the test by themselves
Compal KS | Yes | Yes | Based on customer requirement
Quanta CQ | Yes | Yes | Test parameter: ‐20ºC (0%RH) to +65ºC (40%RH), 1 hour dwell per cycle at each extreme. Temp transition time: < 3min, total 10 cycles.
Pega CQ | Yes | Yes | Based on customer requirement
Compal CQ | Yes | Yes | Based on customer requirement

## Slide 29: Test & Qualification Requirement(2 Of 9)
Few customers conduct 3-point bend test.
 | If the answer is Yes, do you conduct 3-Point bend test? | If the answer is Yes, what is the 3-Point bend test condition, sample size and pass/fail criteria
LCFC | No | NA
Compal CD | No answer | No answer
HuaQin | No | NA
Inventec CQ | No | NA
MSI | No | NA
Pega SZ | No | NA
Compal KS | Yes | Based on customer requirement
Quanta CQ | Yes | Bend Load: Initial force is 10N; Max force is 100N, Incremental load with the rate of 10N/s Bend cycles: 10 cycles
Pega CQ | Yes | 1. Push force: 100N; 2. Test cycle: 10 times for +X axis, both top and bottom side; 3. Pause time (with loading): 1 sec; 4. Speed: 50~100 mm/min; 5. Support axis: 2 end of long edge/short edge 6. Quantity:8; 7. Conduct D&P, X-section
Compal CQ | No answer | No answer

## Slide 30: Test & Qualification Requirement(3 Of 9)
Most ODMs conduct drop test.
 | If the answer is Yes, do you conduct drop test? | If the answer is Yes, what is the drop test condition, sample size and pass/fail criteria
LCFC | Yes | System level only, follow Lenovo's requirement
Compal CD | No answer | No answer
HuaQin | Yes | Test condition: board with foam package, dropped on steel plate from 15 cm and 45 cm height, dropped on wood plate from 45 cm height. 8 corners, angle A: 20° in vertical, angle B: 45° in horizontal. After dropping, conduct function test. Mainly based on customer's requirement.
Inventec CQ | Yes | Based on customer requirement
MSI | Yes | PCBA assembled on station，210 G’s (+/- 10%)，3ms duration，6 faces. Failure criteria: function fail
Pega SZ | Yes | Based on customer requirement
Compal KS | Yes | Based on customer requirement
Quanta CQ | Yes | Operating Half sine wave shock: 40G, 2 ms duration Non‐operating Half sine wave shock: 240G, 2 ms duration Square wave shock: 100G, 180 in/sec velocity change Square wave shock: 150G, 180 in/sec velocity change
Pega CQ | Yes | Based on customer requirement
Compal CQ | No answer | No answer

## Slide 31: Test & Qualification Requirement(4 Of 9)
 | What reliability tests have you performed on the adhesive you use in HVM on the Intel BGA device? | If yes, please provide sample size, temperature cycling profile, G level and number of drops
LCFC | Yes, follow Lenovo's requirement | System level only, follow Lenovo's requirement
Compal CD | DQA will conduct the test, no further information | DQA will conduct the test, no further information
HuaQin | Drop test, shock test | System level drop test: 1 corner/3 edges/6 faces/910 mm height; vibration test:120G/3ms, 6 faces, 3 times/face
Inventec CQ | Yes, based on customer requirement | Based on customer requirement
MSI | After shock test and drop test, conduct D&P | Conduct D&P test after vibration test and drop test Vibration: Frequency: 5-500Hz, test axis: X, Y, Z axis, test duration: 30minutes per axis Drop: Height(cm) 30cm, four edges and six faces
Pega SZ | Yes, based on customer requirement | Based on customer requirement
Compal KS | Based on customer requirement | Based on customer requirement
Quanta CQ | No reliability test on the adhesive | NA
Pega CQ | Detail in right cell | PCB go through 1,2,3 test, then inspect whether any oxidation, corrosion on the surface, conduct function test: 1. TCT630 cycles:-40°C-100°C，rate:15°C-30°C/min, dwell 15-30 min, 600 circles, 2. Free drop: dropped 11 times from 80cm height to concrete floor 3. 85℃/85% RH, dwell 500 hour
Compal CQ | No reliability test on the adhesive | NA

## Slide 32: Test & Qualification Requirement(5 Of 9)
 | Do you conduct other reliability test? Please specify | If the answer is Yes, what is the test condition, sample size and pass/fail criteria
LCFC | No more test on PCBA, based on Lenovo's requirement | No more test on PCBA, based on Lenovo's requirement
Compal CD | No answer | No answer
HuaQin | Yes, 85℃/85% RH，I./O connector durability test | Test condition：85℃/85% RH with bias (DC power thru AC/DC)，600 hours Inspection method: Conduct appearance inspection and function test after every 100 hours, choose 1 PC to conduct X-section
Inventec CQ | Yes, ESD test | No answer
MSI | No | NA
Pega SZ | Based on customer requirement | Based on customer requirement
Compal KS | Based on customer requirement | Based on customer requirement
Quanta CQ | Based on customer requirement | Based on customer requirement
Pega CQ | No | NA
Compal CQ | No answer | No answer

## Slide 33: Test & Qualification Requirement(6 Of 9)
5/10 ODMs follow Intel BFI for In-Circuit Test of PCBA.
 | For In-Circuit Test of PCBA, are Test fixture probes qualified to meet a max strain (ue) Board Flexure Limit. If Yes, please state Max. uE strain value | For Functional Tests of PCBA, what does the test routine cover? How long does the test take?
LCFC | Based on Lenovo’s requirement | Interface function, MAC, depends on different products, less than 10 min
Compal CD | <350 uE | Power-on test, full load test, system basic function test, around 15 min/Pc
HuaQin | ≤450 uE | Full function test, 6-10 min/pc, based on different items and configurations
Inventec CQ | ≤450 uE | Power-on test, 3D mark test
MSI | ≤450 uE | Power-on test, full load test, around 15 min/Pc
Pega SZ | <350 uE | Board function test, around 5 min/PC
Compal KS | ≤450 uE | Power-on test, full load test, Windows function test
Quanta CQ | ≤450 uE | Power-on, function, I/O test, 15 min/Pc
Pega CQ | ＜500 uE | Board level power on-off test, 2-3 min/pc
Compal CQ | No answer | No answer

## Slide 34: Test & Qualification Requirement(7 Of 9)
Most ODMs conduct periodic Rel qualification based on different requirements.
 | Beyond the initial Qualification (Reliability Test), are there periodic subset Reliability qualifications carried out as a mean to verify stability or if there was a major process change post NPI | If yes, how often is this carried out and/or what would initiate this Re-Qualification activity
LCFC | Yes | Follow Lenovo's requirement
Compal CD | Yes | Based on the process change
HuaQin | Yes | Key parts change, PCBA version update, major quality abnormality
Inventec CQ | Yes | Conduct every 6 months, part change and new material change will also initiate the test
MSI | No | NA
Pega SZ | Yes | Based on customer requirement
Compal KS | Based on customer requirement | Based on customer requirement
Quanta CQ | Yes | Only big change happens, based on customer requirement
Pega CQ | Based on customer requirement | Based on customer requirement
Compal CQ | Yes | Only big change happens, like footprint change, PCB design change

## Slide 35: Test & Qualification Requirement(8 Of 9)
Most ODMs don’t conduct Rel test for PCBAs with reworked BGAs.
 | Do you perform reliability test for PCBAs with reworked BGAs(remove and replace)? | If Yes, what is sample size? | If Yes, is it 1x rework or 2x rework activity?
LCFC | Depends, not for every batch | Follow Lenovo's requirement | 1x rework
Compal CD | No, only conduct full function test | NA | NA
HuaQin | NO | NA | NA
Inventec CQ | NO | NA | NA
MSI | NO | NA | NA
Pega SZ | Only for NPI | Based on customer's request, 30~60pcs. | 1~3 x rework
Compal KS | No, only conduct function test | NA | NA
Quanta CQ | No | NA | NA
Pega CQ | No | NA | NA
Compal CQ | No, only conduct function test | NA | NA

## Slide 36: Test & Qualification Requirement(9 Of 9)
 | Please state FA capabilities (destructive/non-destructive) available within your factory campus location?
LCFC | X-ray, D&P, X-section， SEM， EDS
Compal CD | X-section, D&P，2D X-ray
HuaQin | X-RAY, Cross section, Dye&Pry, SEM/EDS, pull test
Inventec CQ | X-RAY, Cross section, Dye&Pry
MSI | X-RAY, Cross section, Dye&Pry, SEM/EDS
Pega SZ | X-RAY, Cross section, Dye&Pry
Compal KS | X-RAY, Cross section, Dye&Pry
Quanta CQ | X-RAY, Cross section, Dye&Pry
Pega CQ | X-RAY, Cross section, Dye&Pry
Compal CQ | X-RAY, Cross section, Dye&Pry
All ODMs have X-RAY, Cross section, Dye&Pry. 3/10 ODMs have SEM/EDS.

## Slide 37: PCB Related

## Slide 38: PCB Related(1 Of 4)
Some ODMs design gold pad for polarity mark on board.
 | For pitch less than or equal to 0.4 mm BGA, do you have requirement to use BGA outline silkscreen? | If yes, is there a print issue(paste volume variation, bridging)? | If silkscreen is not used, do you use exposed copper marking or other board markings?
LCFC | Yes | Yes | No
Compal CD | Yes | No | No
HuaQin | Yes | No | Yes
Inventec CQ | Yes | Yes, SBB risk | No
MSI | Yes | No | NA
Pega SZ | No | NA | Yes, a little Gold pad for polarity mark.
Compal KS | Yes | Yes | Yes
Quanta CQ | Yes | Silkscreen will influence solder paste printing, especially on small size part | Yes
Pega CQ | Yes | No | RD consider to use gold pad for polarity mark
Compal CQ | Yes | No | NA

## Slide 39: PCB Related(2 Of 4)
 | At board and/or system level manufacturing test, do you test the Intel SOC BGA corner NCTF pins for resistance/continuity (checking for solder joint opens), per the MAS guidance in Module 2? (E.G. Yes/No) | What is minimum gap between Solder mask opening and Cu pad in mils/um available without cost adder from PCB manufacturer? | For 0.5 mm pitch and greater BGA, do you prefer to use SMD and/or MD pads in your board design?
LCFC | No | 1.5 mil | MD
Compal CD | No | 1 mil | RD follow Intel recommendation
HuaQin | Yes | 0.5mil | Prefer to design SMD on the corner to increase shock resistance, design MD in the center for better thermal cycle capability.
Inventec CQ | Yes | 2mil | Prefer to design SMD on the corner to increase shock resistance, design MD in other areas
MSI | Yes | 2mil | MD
Pega SZ | No | Different PCB supplier different value, no official information, one supplier provide 1 mil | Based on different products
Compal KS | No | 1.5mil | MD
Quanta CQ | No | Based on supplier's capability, no minimum data | No preference
Pega CQ | No | 1.5mil | Design SMD on the corner to prevent solder joint crack
Compal CQ | No | 1.5mil | MD
3/10 ODMs test the Intel SOC BGA corner NCTF pins for resistance/continuity.

## Slide 40: PCB Related(3 Of 4)
All ODMs can measure reflow oven exit temperature.
 | Are you able to measure the top side PCB temperature, reflow oven exit temperature (at the point when the motherboard exits the reflow oven curtain)? | If yes, what method is used?
LCFC | Yes | Handheld Oven Temp Tester
Compal CD | Yes | Handheld Oven Temp Tester
HuaQin | Yes | Based on reflow profile curve
Inventec CQ | Yes | Handheld Oven Temp Tester
MSI | Yes | Handheld Oven Temp Tester
Pega SZ | Yes | Based on reflow profile curve
Compal KS | Yes | Handheld Oven Temp Tester
Quanta CQ | Yes | Based on reflow profile curve
Pega CQ | Yes | Handheld Oven Temp Tester
Compal CQ | Yes | Handheld Oven Temp Tester

## Slide 41: PCB Related(4 Of 4)
 | What is the minimum PCB thickness for laptop main board that you have experience building in the past? | When attaching thermocouples (TC’s) to BGAs when developing your motherboard reflow profile, do you drill through the board and insert the TC directly into the BGA solder joint? | If No, please describe your process
LCFC | 0.6 mm | Yes | NA
Compal CD | 0.8 mm | Yes | NA
HuaQin | 0.8 mm | Yes | NA
Inventec CQ | 0.6 mm | Yes | NA
MSI | 0.8 mm | Yes | NA
Pega SZ | 0.8 mm | Yes | NA
Compal KS | 0.6 mm | Yes | NA
Quanta CQ | 0.8 mm | Yes | NA
Pega CQ | 0.6 mm | Yes | NA
Compal CQ | 1 mm | Yes | NA

## Slide 43: Clip

## Slide 44: Mark Pad