## Slide 1: Server Customer Summary Report
Prepared by:
SA Moy

## Slide 2: Objectives
Share Findings from CME Server Industry Data Collection Purley/Groveport (SKX, KNL) Platform Survey
    Summarize data collected from the Mobile Customers manufacturers (Quanta, Wistron Zhongshan, Inventec, Foxconn and others)

## Slide 3: Screen Printing

## Slide 4
No | Customer | What is the stencil thickness
 | Quanta | T5.1D19
 | Wistron Zhongshan | T5D19/T6D17
 | Foxconn Tianjin | T4.7D23/T5D19
 | Foxconn Wuhan | T5D19
 | Inventec TAO | T5D19/T4D22
 | Celestica | T5D22
 | Huawei | T5D21/T6D22
 | Compal | T5D19
Stencil Thickness

## Slide 5
No | Customer | Solder Paste used |  |  | 
 |  | Brand | Model | Alloy | Powder Type
 | Quanta | Shenmao | PF606-P | SAC305 | Type 4
 | Wistron Zhongshan | Shenmao | PF606-P | SAC305 | Type 4
 | Foxconn Tianjin | Alpha | OM338-PT | SAC305 | Type 4
 | Foxconn Wuhan | WTO | WTO-LF2000T | SAC305 | Type 4
 | Inventec TAO | Shenmao | PF606-P | SAC305 | Type 4
 | Celestica | Alpha | OM338-PT | SAC305 | Type 4
 | Huawei | Alpha | CVP390 | SAC305 | Type 4
 | Compal | Shenmao | PF606-P | SAC305 | Type 4
Solder Paste

## Slide 6
No | Customer | Please list the Screen Print Machine used | 
 |  | Vendor | Model
 | Quanta | MPM | Momentum
 | Wistron Zhongshan | DEK | Infinity API
 | Foxconn Tianjin | DEK | 265
 | Foxconn Wuhan | DEK | Horizon 03ix
 | Inventec TAO | DEK | Infinity API
 | Celestica |  | 
 | Huawei | DEK | 
 | Compal | DEK | 03ix
Screen Print Machine

## Slide 7
No |  | Pressure | Print Speed | Separation speed
 | Quanta | 16kg | 60mm/s | 0.8mm/s
 | Wistron Zhongshan | 6kg | 50mm/s | 0.5mm/s
 | Foxconn Tianjin |  |  | 
 | Foxconn Wuhan | 12kg | 50mm/s | 2mm/s
 | Inventec TAO | 8kg | 25mm/s | 1.1mm/s
 | Celestica |  |  | 
 | Huawei | 14.8kg | 40mm/s | 1mm/s
 | Compal | 10kg | 80mm/s | 2mm/s
Printing Parameters

## Slide 8: SPI

## Slide 9: SPI Machine
No | Customer | Please list the AOI Machine used | 
 |  | Vendor | Model (Control)
 | Quanta | Cyberoptics | SE500
 | Wistron Zhongshan | Ultra | SE300
 | Foxconn Tianjin | SYMBION | P36
 | Foxconn Wuhan | Orbotech | VT9200
 | Inventec TAO | TR | 7000LL
 | Celestica |  | 
 | Huawei |  | 
 | Compal | Cyberoptics | SE500X

## Slide 10: Placement

## Slide 11
No | Customer | Please list the BGA Placement Machine used | 
 |  | Vendor | Model
 | Quanta | Panasonic | DT401-F
 | Wistron Zhongshan | Panasonic | DT401-F
 | Foxconn Tianjin | Universal | GSM Genesis
 | Foxconn Wuhan | Universal | Genesis
 | Inventec TAO | Fuji | NXT
 | Celestica | Fuji | NXT M6
 | Huawei | SIMENS | 
 | Compal | Panasonic | NPN-W
BGA Placement Machine

## Slide 12: Reflow

## Slide 13
No | Customer | Q1: Reflow Machine's |  | Q2: N2 reflow? | Q3: O2 ppm level
 |  | Brand | Model |  | 
 | Quanta | TAMURA | TNR50-6910PH | Yes | 4000ppm
 | Wistron Zhongshan | TAMURA(FURUKAWA) | TNC51-6212EM | Yes | <500ppm
 | Foxconn Tianjin | Vitronix | XPM 1240 | Yes | <350ppm
 | Foxconn Wuhan |  |  | No | 
 | Inventec TAO | Heller | 1902 | Yes | <3000ppm
 | Celestica | BTU Pyramax | 150N | Yes | <200ppm
 | Huawei | ERSA | 320 | No | 
 | Compal | Heller | 2043 MK5 | Yes | <3000ppm
Reflow Machine, N2 and O2 ppm Level

## Slide 14
No | Customer | With Pallet / Carrier? |  | 
 |  | Yes / No | Product specific / generic pallet? | What material used for Pallet fabrication?
 | Quanta | Yes | Generic | Aluminum
 | Wistron Zhongshan | No |  | 
 | Foxconn Tianjin |  |  | 
 | Foxconn Wuhan |  |  | 
 | Inventec TAO | Yes | Generic SMT carrier | Aluminum Alloy
 | Celestica | Yes | Generic SMT carrier | 
 | Huawei | Yes | Generic | Aluminum alloy
 | Compal | Yes | Generic | Aluminum
Reflow Pallet and Material

## Slide 15
No | Customer | Belt Speed (cm/minute)
 | Quanta | 80cm/min
 | Wistron Zhongshan | 85 – 95cm/min
 | Foxconn Tianjin | 80 cm/min
 | Foxconn Wuhan | 80 cm/min
 | Inventec TAO | 64 – 73 cm/min
 | Celestica | 81 cm/min
 | Huawei | 76cm/min
 | Compal | 85 cm/min
Belt Speed

## Slide 16
No | Customer | Peak temperature (°C) | TAL | Soak Time | Max Rising Slope | Max Falling Slope
 | Quanta | 237.4 – 247 | 68 – 82s | 69 – 88s | 2.25C/s | -2.17C/s
 | Wistron Zhongshan | 236 - 246 | 65 – 83s | 70 – 90s | 0.85C/s | -0.82 C/s
 | Foxconn Tianjin | 235 - 248 | 87 – 116s | 64 – 93s | 2.23C/s | -1.56C/s
 | Foxconn Wuhan | 238 - 246 | 71 – 99s | 75 – 86s | 1.57C/s | -0.86C/s
 | Inventec TAO | 235 - 249 | 59 – 96s | 65 – 96s | 1.5C/s | -0.9C/s
 | Celestica | 236 – 254 | 75-81s | 85-92S | 1.5 C/s | -1.76 C/s
 | Huawei | 237 - 249 | 63-90s | 89s – 92s | 2.2 C/s | -1.6 C/s
 | Compal | 240 - 242 | 81 – 95s | 95 – 100s | 1.3 C/s | -2.2 C/s
Reflow Profile Parameters

## Slide 17: Rework

## Slide 18
Attributes | Quanta | Wistron Zhongshan | Foxconn Wuhan | Inventec TAO | Celestica
Rework Equipment |  |  |  |  | 
Rework Brand | VJE | VJE | VJElectronix | Onyx | VJE
Rework Model | SRT 1800 | SRT1800 | Summit 1800 | 29 | SRT 1800
Nozzle Size | 918mm *663mm | 68mm X 93mm | 88x65 64x43.5 | Confidential | 
Type of Nozzle Design for BGA (Conventional or Center Air flow) | Center air flow | Center Air flow | conventional | Conventional | Center airflow
PnP Process (Manually or Auto) | Auto | Auto | auto | Auto | Auto
Using Nitrogen (Yes or No) | Yes | Yes | no | No | No
Automatic or manual contact solder removal. (Scavenging) | mamual | Manual contact solder removal | Manual | Auto scavenging | Manual
Rework Profile Attribute |  |  |  |  | 
TAL (time above 220 C in sec) | 98~134 / 148~180 | 85s~124s | 60~120 | 100-120s | 74 – 125s
Max Peak Temperature (deg C) | 245℃ / 243℃ | 236°C~243°C | 240+-5 | 243 | 247.2C
Soak time (s) | 82~93 / 93~109 | 66s~78s | 110s | 105-110 | 62 – 73s
Rising Ramp Rate below 205°C | 0.4~0.5 / 0.4 | 0.3°C/s~0.4°C/s | <3c/s | 0.4C/s | 0.4C/s
Critical Rising Ramp Rate between 205°C and 215°C | 0.35~0.5 / 0.35~0.4 | 0.2°C/s~0.3°C/s | <3c/s | 0.57C/s | 0.3C/s
Falling Ramp Rate | 1.0~1.1 / 0.5 | 0.5°C/s~0.9°C/s | <3c/s | -1.64C/s | -0.56 C/s
Board Support |  |  |  |  | 
Board support pins | 3 |  | yes | Yes | Yes
Custom Pallet of fixture for handling | No |  | yes | No | Yes
Sliding suppot with pins | Yes |  | yes | Yes | Yes
Printing Paste / Flux |  |  |  |  | 
Print Paste with mini stencil? | Yes | Yes | yes | Yes | Yes
Do you apply flux to PCB or CPU? | No | Apply flux to PCB for site dressing |  | Desoldering only | No
Print Paste to PCB or CPU? | PCB | PCB | PCB | CPU | PCB
Mini-stencil dimension on "x" and "y". | 85mm*60mm | For half SKT:38.5*52.5mm; For 2 halves SKT:78.5*54.5mm | 55mmx40mm |  | 
Mini-stencil thickness | 0.13mm | 5mil | 5mil | 5mil | 5mil
Mini-stencil aperture shape | 19mil | 19mil | round | 12mil round (CPU) | 19mil
Solder Paste Brand and Model | SHENMAO PF606-P | SHENMAO PF606-P | 维特偶 WTO-LF2000T | Shenmao PF606-P | Alpha OM338 PT
Flux Brand and Model | NA | SHENMAO SMF-2 | RM938 | Shenmao SMF-2 | 
Solder Iron Information |  |  |  |  | 
Solder Type and Alloy | SHENMAO FP606-R,Sn96.5Ag3Cu0.5 | SHENMAO PF606-R(SAC305) | QUICK 203H (sac305) | SAC305 | SAC 305
Solder Iron Temperature | 410℃ | 385±10℃ | 400+-10 | 400C | 
Solder Iron Tip Shape | Knife | Blade Type |  | Blade type | 
Solder Iron Tip Condition | Good | High-frequency Welding |  |  | 
Clean and Tined (Yes/No) | Yes | Yes |  | Yes | 
Contaminated with Burnt Flux (Yes/No) | Yes | No | no | No | 
Flux Information |  |  |  |  | 
Flux Type/Make | NA | Paste Flux (SHENMAO SMF-2) | RM938 | Shenmao SMF-2, NO-CLEAN | 
How is the Flux Applied | NA | ESD Brush |  | BRUSH | 
The Amount of Flux Applied | NA | Uniformity |  | Thin layer | 
The Frequency the Flux is Applied between De-Soldering | NA | Once (before de-soldering) |  | Once | 
Solder Wick Information |  |  |  |  | 
Solder Wick Type | Gootwick | N/A | CP-3015 | Chemtronics Cu | 
Solder Wick Thickness | 0.3mm | N/A | 0.29MM | 0.3mm | 
Solder Wick Width | 2.0mm | N/A | 3.0MM | 2.5mm |