## Slide 1: Server ODM Equipment Survey REport
Ww30 2018
Customer Q&R

## Slide 2: Objective
Share Findings from CME Server Industry Data Collection for Whitley Platform Survey
    Summarize data collected from the Mobile Customers manufacturers (Quanta, Wistron Zhongshan, Inventec, Foxconn and others)
    Green highlighted boxes are updated information from 2018

## Slide 3: Screen Printing

## Slide 4
No | Customer | What is the stencil thickness | Updated Stencil Thickness
 | Quanta | T5.1D19 | 5 mil
 | Wistron Zhongshan | T5D19/T6D17 | T5D19
 | Foxconn Tianjin | T4.7D23/T5D19 | T5D21
 | Foxconn Wuhan | T5D19 | 
 | Inventec TAO | T5D19/T4D22 | T5D19/T4D22
 | Celestica | T5D22 | 
 | Huawei | T5D21/T6D22 | 
 | Compal | T5D19 | 
Stencil Thickness

## Slide 5
No | Customer | Updated Solder Paste used 2018 |  |  | 
 |  | Brand | Model | Alloy | Powder Type
 | Quanta | Shenmao | PF606-P | SAC305 | Type 4
 | Wistron Zhongshan | Shenmao | PF606-P | SAC305 | Type 4
 | Wistron Zhongshan | Henkel | GC10 | SAC305 | Type 4
 | Wistron Zhongshan | Indium | 8.9HF1 | SAC305 | Type 4
 | Foxconn Tianjin | Alpha | OM338-PT | SAC305 | Type 4
 | Foxconn Wuhan |  |  |  | 
 | Inventec TAO | Shenmao | PF606-P | SAC305 | Type 4
 | Celestica |  |  |  | 
 | Huawei |  |  |  | 
 | Compal |  |  |  | 
Solder Paste
No | Customer | Solder Paste used |  |  | 
 |  | Brand | Model | Alloy | Powder Type
 | Quanta | Shenmao | PF606-P | SAC305 | Type 4
 | Wistron Zhongshan | Shenmao | PF606-P | SAC305 | Type 4
 | Foxconn Tianjin | Alpha | OM338-PT | SAC305 | Type 4
 | Foxconn Wuhan | WTO | WTO-LF2000T | SAC305 | Type 4
 | Inventec TAO | Shenmao | PF606-P | SAC305 | Type 4
 | Celestica | Alpha | OM338-PT | SAC305 | Type 4
 | Huawei | Alpha | CVP390 | SAC305 | Type 4
 | Compal | Shenmao | PF606-P | SAC305 | Type 4

## Slide 6
No | Customer | Please list the Screen Print Machine used |  | Please list the new Screen Print Machine used, if different Updated | 
 |  | Vendor | Model | Vendor | Model
 | Quanta | MPM | Momentum | DEK | Horizon 03ix
 | Wistron Zhongshan | DEK | Infinity API | DEK | Infinity API; NeoHorizon; Horizon
 | Foxconn Tianjin | DEK | 265 | DEK | Horizon 03i
 | Foxconn Wuhan | DEK | Horizon 03ix |  | 
 | Inventec TAO | DEK | Infinity API | DEK | Infinity API
 | Celestica |  |  |  | 
 | Huawei | DEK |  |  | 
 | Compal | DEK | 03ix |  | 
Screen Print Machine

## Slide 7
No |  | Pressure | Print Speed | Separation speed
 | Quanta | 14kg | 40mm/s | 20mm/s
 | Wistron Zhongshan | 7-10kg | 30-50mm/s | 0.5mm/s
 | Foxconn Tianjin | 11kg | 50mm/s | 0.5mm/s
 | Foxconn Wuhan |  |  | 
 | Inventec TAO | 13kg | 35mm/s | 0.5mm/s
 | Celestica |  |  | 
 | Huawei |  |  | 
 | Compal |  |  | 
Printing Parameters
No |  | Pressure | Print Speed | Separation speed
 | Quanta | 16kg | 60mm/s | 0.8mm/s
 | Wistron Zhongshan | 6kg | 50mm/s | 0.5mm/s
 | Foxconn Tianjin |  |  | 
 | Foxconn Wuhan | 12kg | 50mm/s | 2mm/s
 | Inventec TAO | 8kg | 25mm/s | 1.1mm/s
 | Celestica |  |  | 
 | Huawei | 14.8kg | 40mm/s | 1mm/s
 | Compal | 10kg | 80mm/s | 2mm/s

## Slide 8: SPI

## Slide 9: SPI Machine
No | Customer | Please list the AOI Machine used |  | Please list the new AOI Machine used, if different Updated | 
 |  | Vendor | Model (Control) | Vendor | Model (Control)
 | Quanta | Cyberoptics | SE500 | Cyberoptics | SE500
 | Wistron Zhongshan | Ultra | SE300 | Cyber Optics TRI | SE500 TR7007 (L)
 | Foxconn Tianjin | SYMBION | P36 | KY | 8030 XL
 | Foxconn Wuhan | Orbotech | VT9200 |  | 
 | Inventec TAO | TR | 7000LL | TRI | 7700SIII/7700SII/7500
 | Celestica |  |  |  | 
 | Huawei |  |  |  | 
 | Compal | Cyberoptics | SE500X |  | 

## Slide 10: Placement

## Slide 11
No | Customer | Please list the BGA Placement Machine used |  | Please list the BGA Placement Machine used, if different Updated | 
 |  | Vendor | Model | Vendor | Model
 | Quanta | Panasonic | DT401-F | Fuji | AIMX-III
 | Wistron Zhongshan | Panasonic | DT401-F | Panasonic | DT401; CM602-F0; NPM
 | Foxconn Tianjin | Universal | GSM Genesis | Panasonic | CM602/BM231
 | Foxconn Wuhan | Universal | Genesis |  | 
 | Inventec TAO | Fuji | NXT | Fuji | NXT II (1190)
 | Celestica | Fuji | NXT M6 |  | 
 | Huawei | SIMENS |  |  | 
 | Compal | Panasonic | NPN-W |  | 
BGA Placement Machine

## Slide 12: Reflow

## Slide 13
No | Customer | Q1: Reflow Machine's |  | Q2: N2 reflow? | Q3: O2 ppm level | Q1: Reflow Machine's |  | Q2: N2 reflow? | Q3: O2 ppm level
 |  | Brand | Model |  |  | Brand | Model |  | 
 | Quanta | TAMURA | TNR50-6910PH | Yes | 4000ppm | Rehm | VXP-9455E690 | Yes | 2500ppm
 | Wistron Zhongshan | TAMURA(FURUKAWA) | TNC51-6212EM | Yes | <500ppm | Rehm | VXP-944, VXP945 (N) | Yes | <500ppm
 | Foxconn Tianjin | Vitronix | XPM 1240 | Yes | <350ppm | Vitronix | XPM 1240 | Yes | <1000ppm
 | Foxconn Wuhan |  |  | No |  |  |  |  | 
 | Inventec TAO | Heller | 1902 | Yes | <3000ppm | Rehm | RS-35319 | Yes | <1000ppm
 | Celestica | BTU Pyramax | 150N | Yes | <200ppm |  |  |  | 
 | Huawei | ERSA | 320 | No |  |  |  |  | 
 | Compal | Heller | 2043 MK5 | Yes | <3000ppm |  |  |  | 
Reflow Machine, N2 and O2 ppm Level

## Slide 14
No | Customer | With Pallet / Carrier? |  |  | With Pallet / Carrier? |  | 
 |  | Yes / No | Product specific / generic pallet? | What material used for Pallet fabrication? | Yes / No | Product specific / generic pallet? | What material used for Pallet fabrication?
 | Quanta | Yes | Generic | Aluminum | Yes | Generic | Aluminum
 | Wistron Zhongshan | No |  |  | Yes when PCB width>250mm | Customized pallet by product | Aluminum
 | Foxconn Tianjin |  |  |  | Yes | Generic | Synthetic stone
 | Foxconn Wuhan |  |  |  |  |  | 
 | Inventec TAO | Yes | Generic SMT carrier | Aluminum Alloy | Yes | Generic SMT carrier | Aluminum Alloy
 | Celestica | Yes | Generic SMT carrier |  |  |  | 
 | Huawei | Yes | Generic | Aluminum alloy |  |  | 
 | Compal | Yes | Generic | Aluminum |  |  | 
Reflow Pallet and Material

## Slide 15
No | Customer | Belt Speed (cm/minute) | Updated Belt Speed (cm/minute)
 | Quanta | 80cm/min | 80 cm/min
 | Wistron Zhongshan | 85 – 95cm/min | 85-95 cm/min
 | Foxconn Tianjin | 80 cm/min | 75 cm/min
 | Foxconn Wuhan | 80 cm/min | 
 | Inventec TAO | 64 – 73 cm/min | 80 cm/min
 | Celestica | 81 cm/min | 
 | Huawei | 76cm/min | 
 | Compal | 85 cm/min | 
Belt Speed

## Slide 16
No | Customer | Peak temperature (°C) | TAL | Soak Time | Max Rising Slope | Max Falling Slope
 | Quanta | 237.4 – 247 | 68 – 82s | 69 – 88s | 2.25C/s | -2.17C/s
 | Wistron Zhongshan | 236 - 246 | 65 – 83s | 70 – 90s | 0.85C/s | -0.82 C/s
 | Foxconn Tianjin | 235 - 248 | 87 – 116s | 64 – 93s | 2.23C/s | -1.56C/s
 | Foxconn Wuhan | 238 - 246 | 71 – 99s | 75 – 86s | 1.57C/s | -0.86C/s
 | Inventec TAO | 235 - 249 | 59 – 96s | 65 – 96s | 1.5C/s | -0.9C/s
 | Celestica | 236 – 254 | 75-81s | 85-92S | 1.5 C/s | -1.76 C/s
 | Huawei | 237 - 249 | 63-90s | 89s – 92s | 2.2 C/s | -1.6 C/s
 | Compal | 240 - 242 | 81 – 95s | 95 – 100s | 1.3 C/s | -2.2 C/s
Reflow Profile Parameters
No | Customer | Peak temperature (°C) | TAL | Soak Time | Max Rising Slope | Max Falling Slope
 | Quanta | 236-248 | 62-76 | 70-95 | 2.1C/s，-2.2C/s | 236-248
 | Wistron Zhongshan | 235 - 245 | 30--120s (60 –90s) | 30--100s (70 – 90s) | 2C/s | -2 C/s
 | Foxconn Tianjin | 235 - 242 | 95 – 110s | 85 – 116s | 2.26C/s | -1.47C/s
 | Foxconn Wuhan |  |  |  |  | 
 | Inventec TAO | 235 - 250 | 60 – 90s | 60 – 120s | 3C/s | 
 | Celestica |  |  |  |  | 
 | Huawei |  |  |  |  | 
 | Compal |  |  |  |  | 

## Slide 17: Rework

## Slide 18
Attributes | Quanta | Wistron Zhongshan | Foxconn Wuhan | Inventec TAO | Celestica
Rework Equipment |  |  |  |  | 
Rework Brand | VJE | VJE | VJElectronix | Onyx | VJE
Rework Model | SRT 1800 | SRT1800 | Summit 1800 | 29 | SRT 1800
Nozzle Size | 918mm *663mm | 68mm X 93mm | 88x65 64x43.5 | Confidential | 
Type of Nozzle Design for BGA (Conventional or Center Air flow) | Center air flow | Center Air flow | conventional | Conventional | Center airflow
PnP Process (Manually or Auto) | Auto | Auto | auto | Auto | Auto
Using Nitrogen (Yes or No) | Yes | Yes | no | No | No
Automatic or manual contact solder removal. (Scavenging) | mamual | Manual contact solder removal | Manual | Auto scavenging | Manual
Rework Profile Attribute |  |  |  |  | 
TAL (time above 220 C in sec) | 98~134 / 148~180 | 85s~124s | 60~120 | 100-120s | 74 – 125s
Max Peak Temperature (deg C) | 245℃ / 243℃ | 236°C~243°C | 240+-5 | 243 | 247.2C
Soak time (s) | 82~93 / 93~109 | 66s~78s | 110s | 105-110 | 62 – 73s
Rising Ramp Rate below 205°C | 0.4~0.5 / 0.4 | 0.3°C/s~0.4°C/s | <3c/s | 0.4C/s | 0.4C/s
Critical Rising Ramp Rate between 205°C and 215°C | 0.35~0.5 / 0.35~0.4 | 0.2°C/s~0.3°C/s | <3c/s | 0.57C/s | 0.3C/s
Falling Ramp Rate | 1.0~1.1 / 0.5 | 0.5°C/s~0.9°C/s | <3c/s | -1.64C/s | -0.56 C/s
Board Support |  |  |  |  | 
Board support pins | 3 |  | yes | Yes | Yes
Custom Pallet of fixture for handling | No |  | yes | No | Yes
Sliding suppot with pins | Yes |  | yes | Yes | Yes
Printing Paste / Flux |  |  |  |  | 
Print Paste with mini stencil? | Yes | Yes | yes | Yes | Yes
Do you apply flux to PCB or CPU? | No | Apply flux to PCB for site dressing |  | Desoldering only | No
Print Paste to PCB or CPU? | PCB | PCB | PCB | CPU | PCB
Mini-stencil dimension on "x" and "y". | 85mm*60mm | For half SKT:38.5*52.5mm; For 2 halves SKT:78.5*54.5mm | 55mmx40mm |  | 
Mini-stencil thickness | 0.13mm | 5mil | 5mil | 5mil | 5mil
Mini-stencil aperture shape | 19mil | 19mil | round | 12mil round (CPU) | 19mil
Solder Paste Brand and Model | SHENMAO PF606-P | SHENMAO PF606-P | 维特偶 WTO-LF2000T | Shenmao PF606-P | Alpha OM338 PT
Flux Brand and Model | NA | SHENMAO SMF-2 | RM938 | Shenmao SMF-2 | 
Solder Iron Information |  |  |  |  | 
Solder Type and Alloy | SHENMAO FP606-R,Sn96.5Ag3Cu0.5 | SHENMAO PF606-R(SAC305) | QUICK 203H (sac305) | SAC305 | SAC 305
Solder Iron Temperature | 410℃ | 385±10℃ | 400+-10 | 400C | 
Solder Iron Tip Shape | Knife | Blade Type |  | Blade type | 
Solder Iron Tip Condition | Good | High-frequency Welding |  |  | 
Clean and Tined (Yes/No) | Yes | Yes |  | Yes | 
Contaminated with Burnt Flux (Yes/No) | Yes | No | no | No | 
Flux Information |  |  |  |  | 
Flux Type/Make | NA | Paste Flux (SHENMAO SMF-2) | RM938 | Shenmao SMF-2, NO-CLEAN | 
How is the Flux Applied | NA | ESD Brush |  | BRUSH | 
The Amount of Flux Applied | NA | Uniformity |  | Thin layer | 
The Frequency the Flux is Applied between De-Soldering | NA | Once (before de-soldering) |  | Once | 
Solder Wick Information |  |  |  |  | 
Solder Wick Type | Gootwick | N/A | CP-3015 | Chemtronics Cu | 
Solder Wick Thickness | 0.3mm | N/A | 0.29MM | 0.3mm | 
Solder Wick Width | 2.0mm | N/A | 3.0MM | 2.5mm | 
Notes: Details of Rework from 2016

## Slide 19
Attributes | Foxconn | Inventec | Quanta | Wistron
Rework Equipment |  |  |  | 
Rework Brand | VJElectronix | ZEVAC | VJE | VJE
Rework Model ID/# | Summit 1800 | Onyx 29 | SRT 1800 | SRT1800, SRT LX
Nozzle Size | For DIMM: 138*10mm； For CPU socket:65*40mm( a half);65*85mm(a set) | Confidential | 68mm *45mm | 68mm X 93mm; Customized by component
Type of Nozzle Design for BGA (Conventional or Center Air flow) | conventional | Conventional | Center air flow | Center Air flow
PnP Process (Manually or Auto) | auto | Auto | Auto | Auto
Using Nitrogen (Yes or No) | no | Yes | Yes | Yes
Automatic or manual contact solder removal. (Scavenging) | Manual | Auto scavenging | mamual | Yes but only being used in special case. Normally, Manual solder removal.
Rework Profile Attribute |  |  |  | 
TAL (time above 220 C in sec) | 60~120 | 60-120s | 60~120sec | 30--120s (60 –90s)
Max Peak Temperature (deg C) | 240+-5 | 250 | 230~250℃ | 235°C~245°C
Soak time (s) | 110s | 60-180s | ≤100sec,maximum≤120sec | 30--100s (70 – 90s)
Rising Ramp Rate below 205°C | <3c/s | 3 deg C/s Max | 0.35~2.5℃/sec | <2°C/s
Critical Rising Ramp Rate between 205°C and 215°C | <3c/s | 3 deg C/s Max | 0.35~0.75℃/sec | <2°C/s
Falling Ramp Rate | <3c/s | 3 deg C/s Max | 0.5~2.0℃/sec | <2°C/s
Board Support |  |  |  | 
Board support pins | yes | Yes | 4 | 
Custom Pallet of fixture for handling | yes | No | No | Yes
Sliding suppot with pins | yes | Yes | Yes | 
Printing Paste / Flux |  |  |  | 
Print Paste with mini stencil? | yes | Yes | Yes | Yes
Do you apply flux to PCB or CPU? | yes, | No | No | Apply flux to PCB for site dressing
Print Paste to PCB or CPU? | PCB | BGA | PCB | PCB
Mini-stencil dimension on "x" and "y". | DIMM socket:13.1*8mm; CPU socket:8*5.9mm&5.8*4.1mm |  | 65mm*50mm | For half SKT:38.5*52.5mm; For 2 halves SKT:78.5*54.5mm; ; Customized by component
Mini-stencil thickness | CPU socket:0.13mm; DIMM socket:0.18mm | 5mil | 0.13mm | 5mil
Mini-stencil aperture shape | For DIMM socket: Resauall. For CPU socket:Round | according to BGA size | 19mil | 19mil
Solder Paste Brand and Model | ALPHA, OM338PT | Shenmao PF606-P | SHENMAO PF606-P | SHENMAO PF606-P
Flux Brand and Model | ALPHA390DH4 | Shenmao SMF-2 | NA | SHENMAO SMF-2
Solder Iron Information |  |  |  | 
Solder Type and Alloy | QUICK 203H (sac305) | SAC305 | SHENMAO FP606-F4,Sn96.5Ag3Cu0.5 | SHENMAO PF606-R(SAC305)
Solder Iron Temperature | 400+-10 | 400C | 410℃ | 385±10℃
Solder Iron Tip Shape |  | Blade type | Knife | Blade Type
Solder Iron Tip Condition |  |  | Good | High-frequency Welding
Clean and Tined (Yes/No) |  | Yes | Yes | Yes
Contaminated with Burnt Flux (Yes/No) |  | No | Yes | No
Flux Information |  |  |  | 
Flux Type/Make | ALPHA390DH4 | Shenmao SMF-2, NO-CLEAN | NA | Paste Flux (SHENMAO SMF-2)
How is the Flux Applied |  | No | NA | ESD Brush
The Amount of Flux Applied |  | No | NA | Uniformity
The Frequency the Flux is Applied between De-Soldering |  | No | NA | Once (before de-soldering)
Solder Wick Information |  |  |  | 
Solder Wick Type | CP-3015 | Chemtronics Cu | Gootwick | N/A
Solder Wick Thickness | 0.29MM | 0.3mm | 0.3mm | N/A
Solder Wick Width | 3.0MM | 3mm | 2.0mm | N/A
Notes: Details of Rework from 2018

## Slide 20: AXI
No | Customer | X-ray Capability | X-ray Machine Brand | X-ray Machine Model | Electrical Test Machine Brand | Eletectrical Test Machine Model | X-y-z alignment measurement (OCMM)
 | Quanta | V810 | ViTrox | S2EX | N/A | N/A | N/A
 | Wistron Zhongshan | 5DX, 2D | Keysight (Aglient); TRI; Phoenix | 5300; TR7600; xlaminar | Agilient | 3070 | AM800CAC
 | Foxconn Tianjin | 3D | Dage | XD7500 | Keyence | VHX-600 | Foxconn/VMS883
 | Foxconn Wuhan |  |  |  |  |  | 
 | Inventec TAO | 2D | YXLON/Unicomp | Y. Cheetah/AX9100 | TRI/Keysight |  | 
 | Celestica |  |  |  |  |  | 
 | Huawei |  |  |  |  |  | 
 | Compal |  |  |  |  |  | 

## Slide 21: Wave solder Parameters
 |  |  | Inventec |  |  | Quanta | 
PROCESS PARAMETER | WAVE SETTINGS |  | CUSTOMER REFERENCE - SET POINTS |  |  |  | 
 | Equipment |  | Electra |  |  | ERSA POWEFLOW N2 XL | 
 | Nitrogen (Y/N) |  | Y |  |  | Y | 
 | If Yes -Oxygen ppm |  | Yes |  |  | ＜2500 | 
CARRIER | Wave Pallet Flow Used (Y/N) |  | Y |  |  | Y | 
FLUXER | Nozzle Fluxer (Set) |  | 0.28mm |  |  | 25% | 
TRANSPORT | Belt Speed (cm/min) |  | 0.9m/min |  |  | 65CM/MIN | 
HEATERS | Upper 1 |  | 385°C |  |  | 240 | 
 | Upper 2 |  | 375°C |  |  | 300 | 
 | Upper 3 |  | 365°C |  |  | 280 | 
 | bottom 1 |  | 400°C |  |  | 220 | 
 | bottom 2 |  | 390°C |  |  | 90 | 
 | bottom 3 |  | 380°C |  |  | 95 | 
 | bottom 4 |  | 335°C |  |  | 240 | 
SOLDER POT | Chip Wave (RPM) |  | 765 |  |  | 1850 | 
 | Smart Wave (Turbulent - RPM) |  | N/A |  |  | 2000 | 
 | Solder Wave (RPM) |  | 910 |  |  |  | 
 | Solder Temperature (Degree °C) |  | 270°C |  |  | 275 | 
 | Lead Clearance (MM/10) |  | 9.0mm |  |  |  | 
 | Back Plate ADJ (MM) |  |  |  |  |  | 
 | Rail Width (mm) |  | 506mm |  |  | 510mm | 
 |  |  |  |  |  | 3 | 
WAVE DWELL TIME (SEC) | Main Wave | Left | 2.4Sec |  |  | 3 | 
 |  | Right | 4Sec |  |  | 4 |